## Slide 1: NAITIONAL TECHNICAL UNIVERSITY OF UKRAINE ”KYIV POLITECHNICAL INSTITUTE” WELDING FACULTY
Presented by: Valerii D. Kuznetsov, D.Sc. (Tech), Professor,
Surface Engineering department, Head
E-mail: kvd@wd.ntu-kpi.kiev.ua
http://weld.kpi.ua

## Slide 2: Table of Content
Introduction Slide #3
Organizational structure of Welding faculty Slides #4
Magnetic control of quality of welded joints
Slides #5-6
Welded joints quality monitoring Slides #7-9
Monitoring of tensions in the pipelines Slides #10-11
Surface engineering |Slides #12-20
Q&A

## Slide 3: Faculty Background
Welding faculty was founded by Boris Paton the president of the National Academy of Science of Ukraine in 1976.
The faculty is the leading post-secondary higher education entity in Ukraine
The educational process is delivered in a close collaboration with the Paton Electric Welding Institute of the National Academy of Sciences of Ukraine.
The best undergraduate students have an opportunity to obtain a European specialist’s certificate.

## Slide 4
.
Organizational structure of Welding faculty
E.O. Paton Electric Welding Institute of NAS of Ukraine
Otto-von-Guericke University (Germany)
Dean
Commission on procedures
Deputy Dean Training and Education
Deputy Dean Scientific Work
Deputy Dean Procedure Work
Methodists of Dean’s Office
Deputy Dean of the Joint Department
Deputy Dean International Relations
.
Welding Production Department
.
Welding Industrial Systems Department
.
Surface Engineering Department
Council of scientists
Department of Graduate Studies
International Institute of Welding
Ukrainian Regional IWE Training Centre
.
Joint Ukrainian-German Department
WF
MEI
FPE
Student’s self-governance
Ukrainian Regional IWE Accreditation

## Slide 5
Magnetic control of quality of welded joints
Wide-bead deposition by welding
Multi-pole system
Single-pole system

## Slide 6
Welding with electro-magnetic effect results in:
Porosity decreasing
Increasing of the resistance to intergranular corrosion
Increasing of the resistance to hot cracking
17 times
12 times
7 times
4 times
1.6 times
2.2 times
2 times
1.7 times
Technologies of welding with electro-magnetic effect are used by the following industrial plants:
۩ Kyiv aircraft building plant; ۩ Frunze Sumy machine engineering productive unit;
۩ Yuzhniy machine engineering plant; ۩ Perm motor engineering complex;
۩ Saratov machine engineering plant; ۩Malyshev Kharkiv plant
۩ Baltia plant;

## Slide 7
Welded joints quality monitoring
Energy transformer
Joint parameters
Construction
Heat dispenser
Welding parameters
Electric parameters of the heating source
Heating source
Control unit
Disturbance
Disturbance
Disturbance

## Slide 8
ADC
Disturbance removal unit
Fragmentation
Parameters calculation
Analysis
Normalization
MAG welding quality monitoring with artificial neural network
Input data
Data processing results
Chart: Accuracy of service, %
| Зміна вильоту | Перевищення кромок | Зміна зазору | Відхилення від стику | Порушення газового захисту | Забруднення кромок
 | 0.96 | 0.95 | 0.925 | 0.95 | 0.9 | 0.92

## Slide 9
Resistance welding quality monitoring with artificial neural network
.
ADC
Filtering
Fragmentation
Analysis
Integrating
Input data
Data processing results
L = 20 – 25 mm, without cracks
L = 12 – 15 mm, with cracks
Basic parameters
Reduced speed
Increased voltage
L = 25 – 30 mm, without cracks
Chart: Accuracy of service, %
| Знижена швидкість рухомої плити | Підвищена напруга | Збільшена швидкість рухомої плити | Збільшений вильот | Коротке замикання
 | 1 | 1 | 1 | 0.95 | 1

## Slide 10: Monitoring of tensions in the pipelines
Magnetic circuit of the electro-magnetic converter
System of electro-magnetic converters
Mechanical tensions measuring system
Monitoring system scheme
Measuring unit

## Slide 11
Installation of the monitoring system

## Slide 12
Surface engineering
WEAR-RESISTANT COATINGS
setting of rail- way switches
SAW deposition
Plasma coating
blade-type and thin base materials
TIG coatings
Hydrogen-oxygen flame
bearing seats
stamp matrix
Ion-plasma method
cutting instrument (razors, needles, etc)

## Slide 13
System for ion-plasma coating of powder materials
Particle of Al2O3 powder plated by titanium and aluminum (x800)
New composite materials with ultra disperse and nano-sized components
Particles of powder after mechanical mixing with aerosyl (x200)
Particle of NiAl powder after plating: r – initial radius, R – radius after h – coating thickness

## Slide 14
LOW EFFICIENCY LAMINIAR PLAZMATRON WHITH ANODE AJUSTED SEPARATEVLY
PLAZMATRON PARAMETERS
working gas .................................................rgon operating current, A ....................................80-120
voltage., V.............................................. to 60
power of plasmatron, kW ......................... to 8,0
flow of gas, l/min.
plasma-forming ........................................ 2,0-3,0 shielding .....................................................1,0-4,0 productivity, kg/h…. ................................. 0,5-4
coated ratio of material .............. . 0, 6-0,8
overall dimensions, mm .................... 140x115x6
THE MAIN PARTS
1- extension anode, 2-hopper, 3- basic nozzle, 4- compressive nozzle, 5- tungsten electrode, 6,9,11 – current pick-up, 7- supply of the plasma-forming gas, 8- mechanism for electrode centering, 9 - supply of cooling water, 10 housing of plasmatron, 12- mechanism for anode displacement

## Slide 15: SURFACE AND MICROSTRUCTURE OF PLAZMA SPRAYED COATINGS
Microstructure of coating on the basis of Al2O3 plated by Ti and Cu (interlayer is not necessary, minimum porosity)
1 –coating, 2-substrate; 3 –interlayer NiAl. (x250)
Surface of plasma coating on the basis of Al2O3
(microscopic cracks are visible )
Surface of plasma coating on the basis of Al2O3 plated by Ti and Cu
(there is no microscopic cracks)
(х 1000)
Microstructure of coating on the basis of Al2O3
(interlayer is necessary )

## Slide 16: PROPERTIES OF PLAZMA SPRAYED COATINGS WHITH UDC
Tensile strength of steel samples with the composite coatings of system AlNi- aL and [PG]-10[Ni]- aL
Kinetics of plasma coatings wear on the basis of plated powders
1 – Al2O3, 2 – Al2O3/Ті/Al

## Slide 17
Application of composite powders with ultra disperse constituents
Restoration of the worn blade for the cut of glass mass by plasma spraying of the Al2O3 powder plated by Ti and Al
у
Plasma spraying of the powder Al2O3, plated by Ti and Cu to the axial supports of the pump impeller for pumping of aggressive liquid
Restoration of the damaged sections of the enamel coatings with plasma spraying of the Al2O3 powder plated by Ti and Al
Plasma spraying of antifriction layer to the bearing surface
the powder [PG]19[M] +[aerosil]
Enamel
Плазменное
покрытие

## Slide 18
Cermet pressure seal of electron-beam gun, made by diffusion welding with the fusible padding
Aviation magnetic valve, obtained by the simultaneous diffusion welding of 5 parts from the different materials
Composite cathodes for the ion-plasma spraying of hafnium, executed by the diffusion welding
а) б)
The exterior view of the surface of heat resistant alloys [CHS]88[U]-[VI] (a) Inconel 718 (b) alloyed by zirconium with the use of high current electron beam
Diffusion technologies in surface engineering