## Slide 1: Characterization of Self-Assembling Quinoline-Based Foldamers by Fluorescence Anisotropy
Jingqi Wang
Supervisor: Prof. Jean Duhamel
May 9, 2018

## Slide 2
Quinoline-based aromatic amide helical foldamer
Q1
Qn
Li, X. Synthesis and Physical Properties of Helical Nanosized Quinoline-Based Foldamers: Dynamic and Photoinduced Electron Transport. Ph.D thesis, University of Bordeaux, 2016.
Foldamers: Artificial folded molecular architectures.
Problems encountered when dealing with Qn
Method for elongating the foldamer into a polymer
Difficult to characterize the size in solution.
Potential methods to solve these problems
Induce polymerization of foldamers by metal complexation.
Characterize the average degree of polymerization of the foldamers by fluorescence anisotropy
Notes: chromophores

## Slide 3: Synthesis of foldamers
Chromatography-free large scale synthesis
Segment doubling synthesis
n
OPV
Qn
Notes: The monomer Q1 produced in Huc’s lab beforehand was reduced to amine by hydrogen with paldium on carbon as catalyst. Meanwhile, another part of Q1 turns into acid through the saponification of ester by NaOH, and subsequently the acid is activated by oxlyl acid. Then the coupling of amine and acid chloride is in the present of the reagent of DIEPA.
. As the oligamer prolong, the activity of nitro group is decreased, so we use ammonium format with pd/c and ammonium matavanadate as catalyst to reduce the nitro group.
problems arise from the low reactivity of the amine end-group and the formation of anhydrides between two acid end groups

## Slide 4: Synthesis of foldamers
OPVQ4
OPVQ7
OPVQ9
OPVQ17
OPVQ24
OPVA
OPVQ4A
OPVQ8A
OPVQ17A
Q8A
Q16A
Q32A

## Slide 5: Complex foldamers with metal coordination
Maurizot, V. Ligation of Helical Foldamers by Metal Coordination. Unpublished. 2017
Meijer, E.W. Reversible Polumers Formed from Self-Complementary Monomers Using Quadruple Hydrogen Bonding. Science 1997, 278,1601-1604.
=0.136nm
Notes: 聊两句 fluorescence
删掉polymer 加decay

## Slide 6: Acknowledgements
Supervisor Prof. Duhamel
Huc’s Group of University of Bordeaux
Other lab members in Duhamel and Gauthier’s Groups
Funding
Bordeaux-Waterloo Research Grant
NSERC