## Slide 1: Probing the Effect of Low Molecular Weight Polymer Diluent on Latex Film Formation by Pyrene Excimer Fluorescence (PEF)
Zehou You
Supervisor: Prof. Jean Duhamel
May 9, 2018

## Slide 2
Film Formation and Oligomer Incorporation
fraction of mixing fm
Soleimani, M.; Khan, S.; Mendenhall, D.; Lau, W.; Winnik, M.A. Polymer 2012, 53, 2652–2663.
Craun, G. P., Rosekelly, G. S., Floyd, F. L. Odor Free, Air Dry, Decorative Latex Paints. U.S. Patent 5,470,906, Nov 28, 1995.
Improving fraction of mixing
  Traditional plasticizers are VOCs that will affect the human body and material quality after evaporation.
  Incorporating Oligomer chains into polymer particles can facilitate film formation.1,2
Two different techniques to probe film formation
  Fluorescence resonance energy transfer (FRET)
  Pyrene excimer fluorescence (PEF)

## Slide 3
Casier, R.; Gauthier, M.; Duhamel, J. Macromolecules 2017, 50, 1635-1644.
Py Py Py* Py (PyPy)* (PyPy)
hν
hν
Py: pyrene
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Pyrene Excimer Fluorescence (PEF1)
IM
IE

## Slide 4
Chart: Annealing time (min)
| 0 | 7 | 15 | 30 | 60 | 120 | 219
 | 0 | 0.65605 | 0.67446 | 0.72554 | 0.75812 | 0.82533 | 0.87162
 | 0 | 0.45038 | 0.53165 | 0.58402 | 0.64005 | 0.70873 | 0.75355
 | 0 | 0.65605 | 0.67446 | 0.72554 | 0.75812 | 0.82533 | 0.87162
 | 0 | 0.27631 | 0.32112 | 0.38742 | 0.41232 | 0.47919
Chart: Annealing time (min)
| 0 | 7 | 15 | 30 | 60 | 120 | 219
 | 0 | 0.20406 | 0.26279 | 0.31395 | 0.37444 | 0.43687 | 0.48277
 | 0 | 0.17254 | 0.2213 | 0.25881 | 0.30007 | 0.38834
94 | 0 | 0.34722 | 0.36361 | 0.41543 | 0.46783 | 0.52919 | 0.59499
 | 0 | 0.20406 | 0.26279 | 0.31395 | 0.37444 | 0.43687 | 0.48277
 | 0 | 0.17254 | 0.2213 | 0.25881 | 0.30007 | 0.38834
 | 0 | 0.3415 | 0.40728 | 0.46352 | 0.52231 | 0.58277 | 0.61817
 | 0 | 0.20406 | 0.26279 | 0.31395 | 0.37444 | 0.43687 | 0.48277
 | 0 | 0.17254 | 0.2213 | 0.25881 | 0.30007 | 0.38834
94 | 0 | 0.34722 | 0.36361 | 0.41543 | 0.46783 | 0.52919 | 0.59499
 | 0 | 0.20406 | 0.26279 | 0.31395 | 0.37444 | 0.43687 | 0.48277
 | 0 | 0.17254 | 0.2213 | 0.25881 | 0.30007 | 0.38834
 | 0 | 0.43812 | 0.4655 | 0.56222 | 0.62973 | 0.68593 | 0.73422
Chart: Wavelength (nm)
Chart: Wavelength (nm)
Steady-state Fluorescence and Fraction of Mixing
seed
seed-oligomer
89 °C
85 °C
89 °C
79 °C
69 °C
83 °C
94 °C
99 °C
106 °C
117 °C

## Slide 5
Chart: fm
| 0.65604887999999995 | 0.67446467499999996 | 0.72553693399999997 | 0.75812430399999997 | 0.82533031099999998 | 0.87162312600000003 | 0.45037592500000001 | 0.531649335 | 0.584019811 | 0.64005080999999997 | 0.70872929100000004 | 0.75354518999999998 | 0.309544706 | 0.359622 | 0.43393879899999999 | 0.46178213899999998 | 0.53677010599999997
 | 0.23312 | -0.063077 | -0.26525 | -0.49998 | -0.64874 | -0.78232 | 0.46181 | 0.29781 | 0.097508 | -0.098215 | -0.26859 | -0.43203 | 0.87589 | 0.68296 | 0.55982 | 0.31945 | 0.17091
 | -2.7669 | -3.0631 | -3.2653 | -3.5 | -3.6487 | -3.7823 | -2.5382 | -2.7022 | -2.9025 | -3.0982 | -3.2686 | -3.432 | -2.1241 | -2.317 | -2.4402 | -2.6806 | -2.8291
 | -0.74818 | -0.78605 | -0.9208 | -1.0567 | -1.1985 | -1.2665 | -0.78401 | -0.89479 | -1.0559 | -1.2233 | -1.3072 | -0.89591 | -1.0013 | -1.1412 | -1.2793 | -1.4337 | -1.5967 | -0.94421 | -1.2324 | -1.4077 | -1.5933 | -1.7695 | -1.8519 | -1.2121 | -1.3781 | -1.554 | -1.7346 | -1.9189 | -2.0609 | -1.4752 | -1.7469 | -1.8542 | -2.0278 | -2.2228 | -2.4294 | -1.6636 | -1.8774 | -2.0527 | -2.2445 | -2.4721 | -2.6515
 | -1.7482 | -1.786 | -1.9208 | -2.0567 | -2.1985 | -2.2665 | -1.784 | -1.8948 | -2.0559 | -2.2233 | -2.3072 | -1.8959 | -2.0013 | -2.1412 | -2.2793 | -2.4337 | -2.5967 | -1.9442 | -2.2324 | -2.4077 | -2.5933 | -2.7695 | -2.8519 | -2.2121 | -2.3781 | -2.554 | -2.7346 | -2.9189 | -3.0609 | -2.4752 | -2.7469 | -2.8542 | -3.0278 | -3.2228 | -3.4294 | -2.6636 | -2.8774 | -3.0527 | -3.2445 | -3.4721 | -3.6515
Chart: fm
| 0.65604887999999995 | 0.67446467499999996 | 0.72553693399999997 | 0.75812430399999997 | 0.82533031099999998 | 0.87162312600000003
 | 1.7105 | 0.86481 | 0.54293 | 0.31624 | 0.22452 | 0.16507
 | 0.67613 | 0.46349 | 0.29224 | 0.18621 | 0.12579 | 0.086338
 | 0.30058 | 0.19276 | 0.14517 | 0.083466 | 0.059288


Chart: fm
| 0.20405643200000001 | 0.26278891799999998 | 0.31395096700000003 | 0.374442161 | 0.43687394699999998 | 0.48276824200000001
 | 0.12708 | 0.09971 | 0.07225 | 0.05256 | 0.036842 | 0.025311
 | 0.058539 | 0.053651 | 0.039339 | 0.028768 | 0.020756 | 0.017747
 | 0.38321 | 0.19737 | 0.13181 | 0.085969 | 0.057296 | 0.0474
 | 0.090342 | 0.070003 | 0.048305 | 0.032855 | 0.027083
88
83
98 | 0.3699 | 0.25239 | 0.16836 | 0.11106 | 0.072662 | 0.052402
105 | 0.63559 | 0.34 | 0.2656 | 0.1781 | 0.11367 | 0.070633
115 | 0.93012 | 0.56856 | 0.37974 | 0.24417 | 0.14457 | 0.095653
Diffusion Coefficients
seed
(0 wt%)
seed-oligomer
(29.6wt%, 1.9kD)
89 °C
85 °C
83 °C
89 °C
79 °C
69 °C
94 °C
99 °C
106 °C
117 °C
seed
(0 wt%)
seed-oligomer
(29.6wt%, 1.9kD)

## Slide 6
Conclusions
Pyrene-labeled latex particles were synthesized and latex films were prepared by combining 95 wt% non-labeled latex with 5 wt% pyrene labeled latex.
The non-labeled latex contained oligomers to enhance polymer diffusion in the latex films during annealing.
Polymer diffusion was monitored as a function of temperature. The presence of oligomer enhanced substantially polymer diffusion.
Future Work
More non-fluorescent labeled latex particles must be prepared with varied contents of oligomers and the impact that the oligomer content has on polymer diffusion in the latex films will be quantified.
Acknowledgements
Jean Duhamel
Remi Casier
Members of the Duhamel and Gauthier groups
NSERC for funding