## Slide 1: New Conjugated Building Block IBDP For Organic Solar Cell
Xiaocheng ZHOU, Yinghui HE
Printed Electronic Materials Lab, Department of Chemical Engineering
2018 IPR Symposium
MAY. 09.2018

## Slide 2: Background for IBDP:
Chem. Commun., 2015, 51, 8093--8096

## Slide 3: IBDP Core Synthesis Scheme:
Yinghui He, et al., Chem. Commun., 2015, 51, 8093--8096
Xiaocheng’s data (Previous PHD Student’s Data)
24.5%
75%
28%
54%

## Slide 4
Synthesis of monomer
Yield：increased from 28% to 44%!
Optimized amount of solvent and catalyst
57%

## Slide 5
Charge transport properties
Polymer | Avg. µe (cm2 V-1 s-1) | Max. µe (cm2 V-1 s-1) | Avg. µh (cm2 V-1 s-1) | Max. µh (cm2 V-1 s-1)
PIBDPBT | 0.048  0.006 | 0.053 | 0.14  0.03 | 0.175
Polymer
Au
Au
DDTS Modified SiO2
N++ doped Si
An ambipolar polymer
High electron and hole mobilities, which are sufficient as acceptor and donor for OPVs, respectively.

## Slide 6: Properties of PIBDPBT
Polymer | λmaxsol/film (nm) | Egopt (eV) | HOMO/LUMO (eV)
PIBDPBT | 699/699 | 1.24 eV | -5.6/-3.7
Cyclic voltammetry: HOMO and LUMO
UV-vis-NIR: band gap

## Slide 7: Preliminary OPV plans: Used as both donor and acceptor in OSCs
-3.2
-5.1
-5.68
-3.7
P3HT
PIBDPBT
E (eV)
Fully covered the range from 400 nm to 1000 nm!
ITO/glass
PEDOT:PSS
Al
P3HT:PIBDPBT
LiF
HT-P3HT is a commercially available donor.
-3.7
-5.68
-5.9
-4.1
PIBDPBT
E (eV)
ITO/glass
PEDOT:PSS
Al
PC71BM:PIBDPBT
LiF
PC71BM
PC71BM

## Slide 8: Future work
Synthesis optimization (New route)
Polymer optimization such as side chains and donor building blocks
Device fabrication

## Slide 9: Acknowledgments
The project is supported by:
Yuning Li, Jenner H.L. Ngai, Arthur D Hendsbee, Han Meng,
Jiaxin Zhu, George Chang, Mozhgan Sadeghianlemraski
Members: