## Slide 1: IMPROVING MMA MONOMER CONVERSION VIA AGET ATRP USING TWO-STEP METHOD IN EMULSION SYSTEM
Presenter: Mohammed Awad
Supervisors: Dr. Ramdhane Dhib and Dr. Thomas Duever
40 IPR Symposium
May 9, 2018

## Slide 2: Overview
Introduction
Experimental Procedure
Results
Next Steps
Acknowledgement

## Slide 3: Results
Table 1: Experimental conditions of emulsion AGET ATRP of MMA @ T=50 oC, MMA-I = 14.04 (g), and MMA-II = 42.12 (g). Mixing speed = 250 rpm.
EBiB (g) | Brij 98 (g) | dNbpy (g) | Ascorbic acid (g) | CuBr2 (g) | N2 Purging
0.4981 | 15.0000 | 0.3065 | 0.0600 | 0.0837 | 10 times for whole emulsion
0.6140 | 22.3820 | 0.2920 | 0.1420 | 0.0800 | 6 times for whole emulsion
Table 2: Experimental results of emulsion AGET ATRP of MMA
Exp. | T (h) | Conv (%) | Mn (g/mol) | Ð
E1 | 1 | 12.1 | 5,719 | 1.19
 | 3 | 24.9 | 6,913 | 1.16
 | 5 | 34.1 | 7,340 | 1.15
E2 | 1 | 37.6 | 13,954 | 1.19
 | 3 | 60.6 | 20,400 | 1.18
 | 5 | 78.2 | 25,216 | 1.17

## Slide 4: Results
Figure 1: (A) Methyl methacrylate (MMA) conversion versus time in emulsion polymerization in experiments E1 and E2 (B) Variations of ln([M]o/[M]) with reaction time in experiments E1 and E2
.
Chart: Time (s)
| 30 | 60 | 120 | 180 | 240 | 300
E2 | 0.34091 | 0.37652 | 0.54231 | 0.66604 | 0.71486 | 0.78201
E1 | 0.097913 | 0.12051 | 0.16675 | 0.18366 | 0.24949 | 0.35416 | 0.34072
Chart: Time (s)
| 30 | 60 | 120 | 180 | 240 | 300
E2 | 0.4169 | 0.4724 | 0.7816 | 1.0967 | 1.2548 | 1.5233
E1 | 0.103 | 0.1284 | 0.1824 | 0.2029 | 0.287 | 0.4372 | 0.4166

## Slide 5: Results
Figure 2: (A) Variations of experimental number-average molar mass versus methyl methacrylate (MMA) conversions (B) Variations of polydispersity index (Ð) versus methyl methacrylate (MMA) conversions in experiments E1 and E2
.
Chart: Conversion (%)
| 38.488 | 49.196000000000012 | 34.091000000000001 | 37.652000000000001 | 54.231000000000002 | 60.604000000000006 | 71.486000000000004 | 78.200999999999993
E2 | 13954 | 20400 | 25216
E1 | 5719 | 6913 | 7340
Chart: Conversion (%)
| 38.488 | 49.196000000000012 | 34.091000000000001 | 37.652000000000001 | 54.231000000000002 | 60.604000000000006 | 71.486000000000004 | 78.200999999999993
E2 | 1.19 | 1.18 | 1.17
E1 | 1.19 | 1.16 | 1.15

## Slide 6: Next Steps
Effects of surfactant, water amount, and mixing speed will be studied.
A model will be developed and kp of this system will be estimated.