## Slide 1: Synthesis of pH-responsive Arborescent Amphiphilic Copolymers for Drug Delivery Applications
Basma Mahi
Supervised by Prof. Mario Gauthier

## Slide 2
Unimolecular Micelles
Hydrophilic
Corona
Hydrophobic
Core

## Slide 3
General Scheme for Arborescent Polymer
Synthesis – Poly(-benzyl L-glutamate) Core
Teertstra and Gauthier, Prog. Polym. Sci. 2004, 29, 277–327

## Slide 4: Research Goal
PBG side chain optimization is necessary to improve the grafting yield
Solution…?
Lactam ring

## Slide 5: Characteristics of Arborescent G0 Obtained with Side Chains Stored Under Different Conditions
Time | Sample | Side Chains | Molar Ratio SC : CO2H | Gy% | PDI
Freshly prepared | G0 G0#1 | Uncapped PDI=1.02 | 1:1.25 1:1.5 | 59 62 | 1.03 1.16
 | G0 G0#3 | Capped PDI=1.07 | 1:1.25 1:1.5 | 69 80 | 1.05 1.60
Stored @RT for 10 days | G0#2 | Uncapped PDI=1.02 | 1:1.5 | 41 | 1.09
 | G0#4 | Capped PDI=1.07 | 1:1.5 | 80 | 1.99
Lower grafting yield expected for side chains stored @RT due to cyclization
Chart: Elution volume (mL)
G0PBG obtained using uncapped side chains, without (blue) and with (red) storage
Chart: Elution Volume (mL)
G0PBG obtained using capped side chains,
without (blue) and with (red) storage
Results

## Slide 6
Capping of the PBG chains with a different amino acid to increase the grafting yield appears to work
L-Lysine may not be the best choice for that purpose
Other amino acids are being investigated
Synthesis of arborescent micelles and targeted delivery will then be investigated
Conclusions