## Slide 1: Compression of Nano‐sized Amylopectin Fragments Probed by Pyrene Excimer Fluorescence (PEF) in DMSO
Damin Kim and Lu Li
Prof. Jean Duhamel
May 9th, 2018

## Slide 2: Outline
Background
- Amylopectin
- Cluster Model
- Pyrene Fluorescence
- Solution Cluster Model (SCM)
Results and Discussion
Conclusions
Future work
Acknowledgements

## Slide 3: Background: Amylopectin
a-1,4 glycosidic bond
a-1,6 glycosidic bond
Properties
Biodegradable
Biocompatible
Non toxic
Economically and environmentally friendly

## Slide 4: Background: Cluster Model
Structural cluster-type models
French
1972
Robin et al.
1974
Manners and Matheson
1981
10 Å
Density of Dry Amylopectin
= 1.5 g/mL
Notes: - Cluster model was introduced around 1970
Amylopectin consist of crystalline and amorphous region
Cluster is the a group of branched chain separated by a linear segments.
- Density of dry amylopectin 1.5 g/mL

## Slide 5: Background: Pyrene Excimer Fluorescence (PEF)
Chart: Wavelength, nm
+
*
*
Large molar extinction coefficient and quantum yield.
Formation of Excimer.
Excimer formation is dependent on
the local concentration and
diffusion coefficient of pyrene.
IE/IM a kdiff [Py]local
tM
tE
IM
IE

## Slide 6: Background: Pyrene Fluorescence
- Sensitive to the local environment
  lifetime
Quenching of Pyrene
Lifetime of pyrene
where RF and RQ are the radii of the fluorophore and quencher and DQ is the diffusion coefficient of a quencher. p is the probability of quenching.
The efficiency of quenching can be described with the bimolecular quenching rate constant, kq

## Slide 7: Background: Pyrene Excimer Fluorescence (PEF)
Chart: Wavelength, nm
+
*
*
tM
tE
IM
IE
Pyrene

## Slide 8: Solution Cluster Model
10 Å
Cluster Model
Solution Cluster Model
What is the distance between helices in solution?
Single Helix
Double Helix
# Anhydroglucose Units Pyrene can see
Dh-h > 34 Å
Effective Distance
16 < Dh-h < 34 Å
Dh-h ~ 27.5 Å
In dilute system
Single Helix
Double Helix
# Anhydroglucose Units Pyrene can see
Notes: Based on hyperchem simulation and fluorescence measurement, the distance between two helices are about 27 .5 angstrom

## Slide 9: Solution Cluster Model
10 Å
Cluster Model
Solution Cluster Model
What is the distance between helices in solution?
Single Helix
Double Helix
# Anhydroglucose Units Pyrene can see
Density= 1.5 g/ml
Radius = 10Å
Density= [NAF (56)], g/mL
Radius =
Notes: Based on hyperchem simulation and fluorescence measurement, the distance between two helices are about 27 .5 angstrom

## Slide 10
Background: Osmotic Pressure
Dilute regime ( C < C*)
Semi Dilute regime (C*< C)
Concentrated Regime(C**< C)
C < C*
C = C *
C**< C
C*** < C
>> 27.5Å
27.5Å
~34Å
27.5Å
27.5Å
>> 34Å
< 34Å
C**:Concentration where dc-c is closer than 34 Å and excimer can be formed b/w two clusters
C***: Concentration where dc-c and dh-h much shorter than 27.5 Å. The short distance restricts the mobility of pyrene
Semi-Dilute regime ( C < C*)
Dense Regime
(C***< C)

## Slide 11: NanoSized Amylopectin Fragments
Amylopectin
NAF(56)
NAF(16)
NAF(8)
Research grade nanosized amylopectin fragments (NAFs) were prepared by Ecosythetix.
~ 200 nm
~ 56 nm
~ 16 nm
~ 8 nm
Notes: In this presentation, compression of the naf will be studied with pef.

## Slide 12: Experimental Conditions
+
Chart: Wavelength, nm
Intramolecular interaction
Chart: Wavelength, nm
Py(0.006%)-NAF(56)
Py(6%)-NAF(56)
IE/IM a kdiff [Py]local
1. Examine the effect of kdiff
2. Examine the effect of IE/IM
What changes does the Cluster experience?
Py Labeled NAFs
Unlabeled NAFs

## Slide 13: Results and Discussion
[NAF (56)]= 53.6 wt%
t= 133 ns
[NAF (56)]
= 0.1 wt%
t= 100 ns
Chart: Wavelength, nm
Experimental Conditions: Py(60ppm)-NAF(56) was mixed with 0-53.6 wt% NAF(56). The amount of Py(60ppm)-NAF(56) was adjusted to get enough fluorescence signal without forming excimer.

## Slide 14: Results and Discussion
Chart: [Py(0.004)-NAF(56)], g/L
| 0.11745247968551499 | 1.1928957492083674 | 4.4032961089370364 | 8.3366342667357323 | 13.64297322726884 | 15.170229190512948 | 4.3461734022550909 | 8.445847743409022 | 16.341446677955588 | 21.932131529827821 | 22.954284272071487 | 36.939284724092296 | 42.270081384722012 | 53.607987494327112
 | 100.1069 | 99.5271 | 100.3974 | 100.7359 | 102.8994 | 103.8254 | 100.8379 | 100.934 | 105.2155 | 110.4581 | 109.5071 | 126.8571 | 133.3151
Experimental Conditions: Py(60ppm)-NAF(56) was mixed with 0-53.6 wt% NAF(56). The amount of Py(60ppm)-NAF(56) was adjusted to get enough fluorescence signal without forming excimer.
where
C*
Regime 1
27.5Å
>> 34Å
27.5Å
< 34Å
11.4 (±0.4) wt%
Local environment of pyrene becomes more viscous
Dilute Regime

## Slide 15: Results and Discussion
Chart: [NAF (56)], wt%
| 5.690681998802994E-2 | 5.8743291814769449E-2 | 9.9835271801527473E-2 | 0.10682480731600177 | 0.64420218037661059 | 0.69907992062060254 | 1.0257913247362254 | 1.0480664980122876 | 2.5703794369645041 | 2.5742202179631719 | 4.9765835659208095 | 5.055078416728902 | 9.2625658423355048 | 9.2743015263768633 | 11.122372537786982 | 11.227946676052619 | 18.865071263846357 | 19.408075264602118 | 26.793131237988966 | 16.752365726137491 | 23.204330613234227 | 28.411897347793403 | 38.55415907128468 | 45.66291334727849 | 54.451941156951648
 | 1 | 0.99631 | 0.99968 | 1.011 | 1.0401 | 1.0236 | 1.0298 | 1.0183 | 1.0536 | 1.0227 | 1.0665 | 1.0409 | 1.143 | 1.1089 | 1.2258 | 1.1192 | 1.4913 | 1.4948 | 1.6773 | 1.355 | 1.6098 | 1.7768 | 2.7873 | 3.2305 | 3.0347
Experimental Conditions: 7.8×10-3 wt% of Py(6%)-NAF(56) was mixed with 0-56 wt% NAF(56)
Chart: Wavelength, nm



C**=16 wt%
1.5wt%
IE/IM a kdiff [Py]local
C***
=46wt%
Solution Cluster Model
10 Å
Cluster Model
Density= 1.5 g/ml
Radius = 10Å
Radius =
Density= [NAF (56)], g/mL
Concentration | Distance
C* | 96.8 Å
C** | 26.1 Å
C*** | 12.9 Å
Effective distance: 16 ~36 Å

## Slide 16: Results and Discussion
Chart: [NAF (56)], wt%
| 5.690681998802994E-2 | 5.8743291814769449E-2 | 9.9835271801527473E-2 | 0.10682480731600177 | 0.64420218037661059 | 0.69907992062060254 | 1.0257913247362254 | 1.0480664980122876 | 2.5703794369645041 | 2.5742202179631719 | 4.9765835659208095 | 5.055078416728902 | 9.2625658423355048 | 9.2743015263768633 | 11.122372537786982 | 11.227946676052619 | 18.865071263846357 | 19.408075264602118 | 26.793131237988966 | 16.752365726137491 | 23.204330613234227 | 28.411897347793403 | 38.55415907128468 | 45.66291334727849 | 54.451941156951648
 | 1 | 0.99631 | 0.99968 | 1.011 | 1.0401 | 1.0236 | 1.0298 | 1.0183 | 1.0536 | 1.0227 | 1.0665 | 1.0409 | 1.143 | 1.1089 | 1.2258 | 1.1192 | 1.4913 | 1.4948 | 1.6773 | 1.355 | 1.6098 | 1.7768 | 2.7873 | 3.2305 | 3.0347
Experimental Conditions: 7.8×10-3 wt% of Py(6%)-NAF(56) was mixed with 0-56 wt% NAF(56)
Chart: Wavelength, nm



16 wt%
1.5wt%
C*
C**
27.5Å
>> 34Å
27.5Å
< 97Å
<~26 Å
Semi dilute Regime
Conc. Regime
IE/IM a kdiff [Py]local
No change in [Py]local
Increase in [Py]local
27.5Å
~12.9Å
C***
46 wt%
Dense Regime

## Slide 17
Experimental Conditions: 7.8×10-3 wt% of Py(6%)-NAF(56) was mixed with 0-56 wt% NAF(56)
Results and Discussion
+
*
Diffusion
Direct excitation
Chart: [NAF(56)], wt%
| 5.690681998802994E-2 | 5.8743291814769449E-2 | 9.9835271801527473E-2 | 0.10682480731600177 | 0.64420218037661059 | 0.69907992062060254 | 1.0257913247362254 | 1.0480664980122876 | 2.5703794369645041 | 2.5742202179631719 | 4.9765835659208095 | 5.055078416728902 | 9.2625658423355048 | 9.2743015263768633 | 11.227946676052619 | 19.408075264602118 | 16.752365726137491 | 23.204330613234227 | 28.411897347793403 | 38.55415907128468 | 42.827880845086874 | 45.66291334727849 | 54.451941156951648
 | 0.78617 | 0.86261 | 0.76591 | 0.77469 | 0.63055 | 0.63624 | 0.87062 | 0.84791 | 0.891 | 0.81099 | 0.8216 | 0.80633 | 0.81934 | 0.84269 | 0.81103 | 0.71044 | 0.82243 | 0.72597 | 0.70959 | 0.57933 | 0.55505 | 0.49265 | 0.48421
 | 0.18536 | 0.12225 | 0.21319 | 0.20194 | 0.15176 | 0.104 | 0.11751 | 0.13312 | 0.097581 | 0.1693 | 0.16258 | 0.17286 | 0.16451 | 0.1455 | 0.16389 | 0.26543 | 0.16313 | 0.24828 | 0.2606 | 0.37682 | 0.39837 | 0.4581 | 0.4682
Excimer formed via diffusion
Formed via Direct Excitation
Chart: [NAF(56)], wt%
| 5.690681998802994E-2 | 5.8743291814769449E-2 | 9.9835271801527473E-2 | 0.10682480731600177 | 0.64420218037661059 | 0.69907992062060254 | 1.0257913247362254 | 1.0480664980122876 | 2.5703794369645041 | 2.5742202179631719 | 4.9765835659208095 | 5.055078416728902 | 9.2625658423355048 | 9.2743015263768633 | 11.122372537786982 | 11.227946676052619 | 18.865071263846357 | 19.408075264602118 | 16.752365726137491 | 23.204330613234227 | 28.411897347793403 | 38.55415907128468 | 42.827880845086874 | 45.66291334727849 | 54.451941156951648
 | 476.0452 | 476.2211 | 476.2533 | 476.0576 | 476.1118 | 476.0776 | 476.1535 | 476.1307 | 476.1007 | 476.2198 | 476.1536 | 476.2747 | 476.3593 | 476.4738 | 476.4635 | 476.5066 | 476.7112 | 476.7623 | 476.7933 | 477.1437 | 477.068 | 476.8137 | 473.1653 | 474.1581 | 472.6206
38 wt%
38 wt%
Chart: Wavelength, nm
[NAF(56)]=0.01wt%
[NAF(56)]= 56 wt%
Max λ
C*
C**
At C**
At C***
27.5 Å
< 26.1 Å
12.9Å
Further increase in h
C**
High quantum Yield
Low quantum Yield
*
Notes: At C*** the distance between helices is too short which results in confining pyrene molecules in a small given area. As pyrene molecules are so close to each other, they will form excimer without having time to reorient themselves. The excimer will be formed with poor orientation. Poor overlapped excimer has low quantum yield.

## Slide 18: Results and Discussion
Chart: Wt%
| 13.333011501009089 | 16.583272211719262 | 16.485572886548514 | 16.403099999999998
 | 200 | 56.75 | 17.23 | 8.27
 | 200 | 56.75 | 17.23 | 8.27
 | 200 | 56.75 | 17.23 | 8.27
Chart: [NAF (56)], wt%
| 0.11465260261407932 | 1.0198374839622331 | 2.0029216036357731 | 3.8717907829692235 | 7.4003327376917865 | 8.8868157332450579 | 16.50450350272434 | 22.896146976269456 | 37.158036150464078 | 43.727563791597959 | 48.303137192026071 | 55.967872486146554
 | 1 | 1.0457 | 1.0487 | 1.0769 | 1.2669 | 1.2307 | 1.748 | 2.4597 | 3.6657 | 2.9419 | 3.2565 | 2.6833
 | 1 | 0.99631 | 0.99968 | 1.011 | 1.0401 | 1.0236 | 1.0298 | 1.0183 | 1.0536 | 1.0227 | 1.0665 | 1.0409 | 1.143 | 1.1089 | 1.2258 | 1.1192 | 1.4913 | 1.4948 | 1.6773 | 1.355 | 1.6098 | 1.7768 | 2.7873 | 3.2305 | 3.0347
 | 1 | 1.0061 | 1.0186 | 1.016 | 1.0883 | 1.1436 | 1.1905 | 1.2297 | 1.4324 | 1.4859 | 1.7156 | 2.0145 | 2.0398 | 2.1838 | 1.9873 | 1.7522
 | 1 | 1.0241 | 1.0437 | 1.0202 | 1.0384 | 1.0352 | 1.1338 | 1.1025 | 1.1736 | 1.2066 | 1.4728 | 1.6258 | 1.9242 | 3.1925
Amylopectin
NAF (56)
NAF(16)
NAF (8)
C*
C**
C***
C***
C**

## Slide 19: Results and Discussion
Chart: Wt%
| 13.333011501009089 | 16.583272211719262 | 16.485572886548514 | 16.403099999999998
 | 200 | 56.75 | 17.23 | 8.27
 | 200 | 56.75 | 17.23 | 8.27
 | 200 | 56.75 | 17.23 | 8.27
C**
27.5Å
>> 34Å
27.5Å
< 34Å
~ 27Å
Semi Dilute Regime
Conc.
Regime
27.5Å
~14Å
C***
Dilute Regime
Dense
Regime
Notes: C* depends on the molecular weight of the particle
C** and C*** relate the cluster and is independent to the size of particle. Compression of helice will start at around 16 wt% for any sized fragments. 40% (4)

## Slide 20: Conclusions
Compressibility of amylopectin and NAFs was studied by Pyrene Excimer Fluorescence (PEF).
  Increase in the concentration of NAFs built up the osmotic pressure which triggers their compression.
  The compression of helice of cluster is independent to the size of fragment and starts around 15.7 (±1.6) wt %

## Slide 21: Future Work
Dispersions with higher concentrations of NAFs in DMSO will be prepared to study the conformation changes experienced by NAFs during film formation.

## Slide 22: Acknowledgements
Prof. Jean Duhamel
Lu Li
All members from Duhamel and Gauthier’s labs
All Ecosynthetix’s project members
22

## Slide 23
Thank You
23

## Slide 24: Results and Discussion
Chart: Wt%
| 13.333011501009089 | 16.583272211719262 | 16.485572886548514 | 16.403099999999998
 | 200 | 56.75 | 17.23 | 8.27
 | 200 | 56.75 | 17.23 | 8.27
 | 200 | 56.75 | 17.23 | 8.27
C*
C**
27.5Å
>> 34Å
27.5Å
< 34Å
< 34Å
Regime 1
Regime 2
27.5Å
>> 27.5Å
C***

## Slide 25
Solution Cluster Model
10 Å
Cluster Model
Radius =
Density= 1.5 g/ml
Density= [NAF (56)], g/mL
Radius = 5Å
C*=0.016 g/mL
C**= 0.22 g/mL
C***=0.90 g/mL
Radius=
= 96.8
Radius =
= 26.1
Radius =
= 12.9

## Slide 26: Results and Discussion
Experimental Conditions: Py(60ppm)-NAF(56) was mixed with 0-53.6 wt% NAF(56). The amount of Py(60ppm)-NAF(56) was adjusted to get enough fluorescence signal without forming excimer.
where
11.4 (±0.4) wt%
C*
At C< C*
At C*
At C**,
11.4 wt%
No Change
Increase in h
27.5 Å
27.5 Å
27.5 Å
> 36 Å
> 36 Å
< 36 Å
Notes: Longer lifetime of pyrene indicates that the local environment of pyrene gets more viscous with increasing [NAF(56)]. This implies that diffusion is hindered at NAF(56) concentration greater than 11.4 (±0.4) wt%.

## Slide 27: Results and Discussion
C**
Concentration where IE/IM begins to increase (= [Py]local begins to increase)
Chart: [NAF (56)], wt%
| 13.64297322726884 | 15.170229190512948 | 16.341446677955588 | 21.932131529827821 | 22.954284272071487 | 42.270081384722012 | 53.607987494327112
 | 102.8994 | 103.8254 | 105.2155 | 110.4581 | 109.5071 | 126.8571 | 133.3151
 | 100.1069 | 99.5271 | 100.8379 | 100.3974 | 100.7359 | 100.934

## Slide 28: Background: Osmotic Pressure
Stage 1: Dilute region ( C < C*)
Stage 2: Semi Dilute region (C = C*)
Stage 3: Concentrated region(C*< C)
C*< C < C**
C**< C < C***
C < C***
C < C*

## Slide 29: Results and Discussion
Chart: [NAF (56)], wt%
| 5.690681998802994E-2 | 5.8743291814769449E-2 | 9.9835271801527473E-2 | 0.10682480731600177 | 0.64420218037661059 | 0.69907992062060254 | 1.0257913247362254 | 1.0480664980122876 | 2.5703794369645041 | 2.5742202179631719 | 4.9765835659208095 | 5.055078416728902 | 9.2625658423355048 | 9.2743015263768633 | 11.122372537786982 | 11.227946676052619 | 18.865071263846357 | 19.408075264602118 | 26.793131237988966 | 16.752365726137491 | 23.204330613234227 | 28.411897347793403 | 38.55415907128468 | 45.66291334727849 | 54.451941156951648
 | 1 | 0.99631 | 0.99968 | 1.011 | 1.0401 | 1.0236 | 1.0298 | 1.0183 | 1.0536 | 1.0227 | 1.0665 | 1.0409 | 1.143 | 1.1089 | 1.2258 | 1.1192 | 1.4913 | 1.4948 | 1.6773 | 1.355 | 1.6098 | 1.7768 | 2.7873 | 3.2305 | 3.0347
Experimental Conditions: 7.8×10-3 wt% of Py(6%)-NAF(56) was mixed with 0-56 wt% NAF(56)
Chart: Wavelength, nm



C*
16 wt%
C**
At C< C*
At C*
At C**, 16 wt%
No Change
Increase in [Py]local
IE/IM a kdiff [Py]local
27.5 Å
> 36 Å
27.5 Å
> 36 Å
27.5 Å
< 36 Å

## Slide 30: Background: Osmotic Pressure
C = C*
C < < C*
C < C*
C = C*
C > C*
What happens to the Cluster?
27.5 Å
> 36 Å
< 36 Å
27.5 Å
< 27.5 Å
< 27.5 Å
IE/IM a kdiff[Py]local
Compression
Increase in [Py]local
Change in local environment of pyrene

## Slide 31: Background: Osmotic Pressure
C < C*
C = C*
C < < C*
Increase in concentration
Stage 1: Dilute region ( C < C*)
Stage 2: Semi Dilute region (C = C*)
Stage 3: Concentrated region(C*< C)
In a dilute system, a polymer is highly swollen.
Partial interpenetration is possible with chains outside a macromolecule
Further interpenetration is prevented by branched segments which results in compression instead.