## Slide 1: Hierarchical Self-Assembly Induced by Dilution-Enhanced Hydrophobic Hydration
Presented by: Dapeng Liu
Supervisor: Xiaosong Wang

## Slide 2
Outline
1. Introduction
2. Dilution-induced self-assembly of Fp(CH2)6Azobenzenetrans MCsomes
3. The conditional effect of hydrophobic hydration
4. Hierarchical self-assembly of MCsomes
5. Summary

## Slide 3
Hydration of hydrophobic solutes
Hydrophobic hydration is the hydration of hydrophobic molecules or surface.
Small solutes
H atom
O atom
Hydrophobic solutes
Large solutes
Nature 437, 640–647
Notes: Hydrophobic hydration involves the minimization of the free energies of water molecules near nonpolar surfaces.

## Slide 4
Hydrophobic hydration in protein chemistry
Hydrophobic hydration plays an important role in protein folding and self-assembly.
J. Am. Chem. Soc. 2017, 139 (49), 17890-17901.
Current Opinion in Colloid & Interface Science 2016, 22, 73-79.
water

## Slide 5
Most model systems in chemical self-assembly are focused on amphiphilic nature instead of the hydrophobic hydration
Chemical self-assembly
Chem. Soc. Rev. 2012, 41 (18), 5969-5985.
Science 294.5547 (2001): 1684-1688.

## Slide 6
Self-assembly in water
[δ-]
[δ+]
FpC6X
Hydrophobic
Fp head
Hydrated
Fp head
[δ-]
Hydration of Fp head
MCsome
C6X tail ( )
FpC6X
FpC6
FpC6Azobenzene
Recently our groups synthesized a series of hydrophobic metal carbonyl complexes which could self-assemble into nanovesicles by hydrated Fp head.
Aqueous self-assembly of hydrophobic molecules FpC6X

## Slide 7
200 nm
a
c
d
Dh = 168 nm
PDI: 0.174
Charaterization of Fp(CH2)6Azobenzenetrans Mcsomes
b
Fp(CH2)6Azobenzenetrans MCsomes with ca. 170 nm were formed.
TEM
AFM
SEM
DLS
1 um
500 nm

## Slide 8
Dilution-induced self-assembly of Fp(CH2)6Azobenzenetrans MCsomes
a
b
c
14 μM
140 μM
Dilution of MCsomes
Time aging
Helical structures
Dilution of Fp(CH2)6Azobenzenetrans MCsomes could induce the self-assembly of MCsomes.
500 nm
500 nm

## Slide 9
1. How does dilution induce self-assembly of FpC6Azobenzenetrans MCsomes?
2. How do FpC6Azobenzenetrans MCsomes transform to helical structures?

## Slide 10
Dilution-induced zeta potential change of Fp(CH2)6Azobenzenetrans MCsomes
Self-assembly in water
FpC6Azobenzenetrans
Hydration of Fp head
MCsome
[δ-]
[δ+]
Hydrated
Fp head
[δ-]
Dilution of Fp(CH2)6Azobenzenetrans MCsomes could cause the surface charge decrease

## Slide 11
The IR spectra of Fp(CH2)6Azobenzenetrans MCsomes during the dilution process
[δ-]
[δ+]
[δ-]
MCsome
No shifts in the wavenumbers for the absorption peaks suggest that the dilution results in no detectable variation in polarized CO groups in the Fp head.

## Slide 12
Potential (V)
Potential (V)
140 µM
70 µM
35 µM
14 µM
ΔE1/2 = 0.20 V
ΔE1/2 = 0.18 V
ΔE1/2 = 0.16 V
CV experiments of Fp(CH2)6Azobenzenetrans MCsomes during the dilution process
[δ-]
[δ+]
[δ-]
MCsome
CV indicates that the dilution could enhance the hydrophobic hydration of Fe in the MCsomes.
dFp-Fp
Hydration cavity
Notes: the close proximity of the adjacent Fp head groups on the surface of colloids results in two oxidation potentials separated by a redox coupling (ΔE1/2) because the oxidation of the iron element next to the oxidized one requires a higher potential

## Slide 13
Calcein quenching experiments verified that the dilution could enhance the hydrophobic hydration of Fe in the MCsomes
Calcein quenching experiments of Fp(CH2)6Azobenzenetrans MCsomes during the dilution process
[δ-]
[δ+]
Hydrated
Fp head
[δ-]
MCsome
More hydration of Fe, more quenching of calcein
Calcein
the Stern-Volmer plot
Notes: The Stern-Volmer plot for the fluorescence quenching of calcein

## Slide 14
O [δ-]
Fe [δ+]
[δ-]
[δ+]
[δ-]
O [δ-]
Fe [δ+]
Zeta potential ζ = -51 mV
ζ = -31 mV
Dilution
Less HH
Increased HH
Water-Carbonyl Interactions
(HH: hydrophobic hydration)
Dilution-enhanced hydrophobic hydration (HH) of Fe in the MCsomes

## Slide 15
How do MCsomes transform to helical structures?

## Slide 16
b
e
f
g
h
a
c
d
Scale bar: 500 nm
TEM was used to track the hierarchical self-assembly of MCsomes
Different intermediates were obtained by TEM during the structural evolution

## Slide 17
The hierarchical self-assembly of MCsomes
Scheme of the hierarchical self-assembly of MCsomes

## Slide 18
20 µm
500 nm
The hierarchical self-assembly of FpC6Azobenzenetrans MCsomes at pH = 3
pH
Zeta potential (mv)
FpC6Azobenzenetrans colloid (140 uM)
FpC6Azobenzenetrans colloid (140 uM, pH=3)
TEM
The hierarchical self-assembly of MCsomes was also observed in the colloid (140 uM) at pH = 3.

## Slide 19
Summary
Hydrophobic FpC6Azobenzene molecules could self-assemble into MCsomes in water by hydration of Fp head.
Dilution could enhance the hydrophobic hydration of Fe in the Fp head which decrease the surface charge of the MCsomes.
The enhanced hydrophobic hydration of Fe could be verified by CV and dye quenching experiments.
The decreasing surface charge could induce hierarchical self-assembly of nanovesicles to helical structures.
The structural evolution from nanovesicles to helical structures could be observed by TEM which proceed through large vesicles, one-dimensional array of vesicles, tubes and helical structures.

## Slide 20
Thank you