## Slide 1: Viscoelastic Properties of Crosslinked Chitosan Edible Films
Joseph Khouri
Supervisors: Profs. C. Moresoli and A. Penlidis
Dept. of Chemical Engineering

## Slide 2
Protein removal
Mineral removal
De-colorization
Base treatment,
NaOH < 5 %, T < 80 oC
Acid treatment,
HCl < 5 %, T ~ RT
Main: Crustaceans (exoskeletal shells), Secondary: Fungi (stem walls), Squid pen, cuttlefish
PRODUCTION
Deacetylation
Base treatment, boiled
NaOH > 40 %, T > 100 oC
Oxidation,
KMnO4 or UV
CaCO2
CaCO2
CaCO2
Chitin  Chitosan conversion
Chitin Sources

## Slide 3
n – glucosamine residue
m – N-acetyl glucosamine residue
DD = degree of deacetylation = 100 % × n
Chitosan = DD > 60 %, or > 7 % nitrogen
Chitin = DD < 60 % or < 7 % nitrogen
STRUCTURE
(1,4)-2-amino-2-deoxy-b-D-glucan
Okuyama et al. Macromolecules, 1997, 30, 5849-5855
Molecular weight commercial chitosan, Mv = 50 to 500 kDa
Units alternate by 180o

## Slide 4
STRUCTURE
Allomorphs
Tendon
- hydrated
- Orthorhombic
- Anti parallel
chain packing
Annealed
Anhydrous
Orthorhombic
anti parallel
packing
Semi-crystalline, 35 – 60 %; two-fold helical conformation (“zig-zag”); strong H-bond network
Yui et al. Macromolecules 1994, 27, 7601 - 7605
tendon ~ 10o
annealed ~ 15o
Okuyama et al. Macromolecules, 1997, 30, 5849-5855

## Slide 5
Membranes/Industrial Technology
Medical/Health
Food
APPLICATIONS
Heavy ion removal from waste water
Flocculating agent
Fuel cell membrane
Hydrogels for drug delivery
Scaffolds for bone regeneration
Hemostatic/
anticoagulant material
Cosmetics
(skin, oral care)
Thickener, stabilizer
Preservative
Appetite suppressant
Coatings/packaging

## Slide 6
Property | Chitosan | Common plastics (LDPE, PP, etc..)
Water Vapor Permeability (WVP) [g/(m-s-Pa)] | 1 – 10 ×10-11 | 0.01 – 1 ×10-11
Oxygen Gas Permeability (OP) [cm3/(m-s-Pa)] | 1 × 10-15 – 1 × 10-13 | 1 × 10-13 – 1 × 10-12
Tensile Strength (TS) [MPa] | 1 – 100 | 1 - 100
Elongation Before Break [%] | 1 – 50, 100 (with plasticizer) | 1 – 1,000
Young’s Modulus [GPa] | 0.1 – 3 | 1 - 10
Processability | Solvent casting, Limited molding | Moldable (thermo-, injection, blow, etc…)
PROPERTIES

## Slide 7
Grafting
Composites
Crosslinking
MODIFICATION
With hydrophobic compounds, lipids (e.g., palmitic, stearic, octanoic, acids):
– Some improvement in gas barrier
– Little to no improvement, in WVP, TS
With polysaccharides:
– No significant change in properties
Objectives for modification: (i) Reduce hydrophilicity, (ii) improve mechanical properties, while (iii) not causing significant changes to gas barrier or antibacterial properties
With hydrophobic compounds, lipids (e.g., stearic acid):
– Some improvement in hydrophobicity, some compromise in TS and antibacterial properties
– Improvement in antioxidation (with gallic acid)
With multifunctional compounds
(e.g., tannic acid);
- Some improvement in TS, WVP, and oxygen permeability
- Some reduction of antibacterial properties

## Slide 8
Glutaraldehyde
CROSSLINKERS
Epichlorohydrin
Genipin
Citric Acid
Tannic Acid
- Waste water treatment applications
- Toxic
- Biomedical applications
- Total health impact / suitability for food applications still unknown
- Improvements in TS, WVP
- Non-toxic
Improvements in TS, WVP
Non-toxic
Not fully studied with chitosan for edible film applications

## Slide 9
CROSSLINKING
Crosslinking with citric acid investigated with:
 | Target application
Starch | Food packaging
Proteins (peanut, …) | Food packaging
Carboxymethyl cellulose – Hydroxyethylcellulose | Superabsorbent hydrogel
Hydroxy propyl methyl cellulose (HPMC) | Food packaging
Chitosan-HPMC composite | Food packaging
Chitosan-Alginate composite | Drug delivery
Chitosan graft on wool, cotton | Textiles
Chitosan, chitosan graft on polyurethane | Food packaging, drug delivery, biomedical applications

## Slide 10
CROSSLINKING
NaH2PO2
105 – 190 oC, 5 min – 6 hours, 5 – 30 % citric acid (w/w), 0 – 15 % catalyst

## Slide 11
FTIR
Rubber Elasticity Theory
E – elastic storage modulus
G – elastic shear modulus
Mc – average molecular weight
between crosslinks
R – gas constant
T – temperature
CROSSLINKING
V – Poisson Ratio
n – crosslink density
r – material density
Reddy and Yang,
Food Chemistry 2010, 118, 702-711

## Slide 12
VISCOELASTICITY
Glass transition temperature, Tg, of chitosan in dispute. Estimates ~ 140 – 200 oC.
Undetectable, weakly observable with DSC
Sakurai Polymer 2000, 21,
7051 - 7056
Preheated chitosan film
chitosan film
Chitosan/poly (N-vinyl
pyrrolidone)
Debate on the nature of the DMA tan(d) peak near 160 oC,
glass transition vs. molecular motion of pseudo-stable state type
E′ – storage modulus
E′′– loss modulus
tan(d) = E′′ /E′

## Slide 13
Neat
Neutralized
Glutaraldehyde (3, 6, 12 % w/w-chitosan), homogeneous and heterogeneous
Citric Acid (15 % w/w-chitosan), with and without heat treatment (HT) (150 oC, 0.5 h)
EXPERIMENTAL
Films prepared from solvent casting with acetic acid (Ac)
NH3+
NH3+
NH3+
NH3+
Ac-
Ac-
Ac-
Ac-
NH2
NH2
NH2
NH2
neutralize
NaOH
Neutralization
Single step,
Chitosan + Ac
+ crosslinker in solution
Heterogeneous Crosslinking
Multistep, prepare film, immerse in aqueous solution with crosslinker
Homogeneous Crosslinking

## Slide 14
Dynamic Mechanical Analysis
DMA Q800 (TA Instruments), tensile clamp
Single Scan
T-range = 30 – 200 oC
q = 3 oC/min
e = 0.15 %
f = 1 Hz
Preheated Scans
Equilibrated at 140 oC / 10 min
Followed by regular scan
EXPERIMENTAL
(http://norleq.com/en/dt_portfolio/q800-dma-2-2/)

## Slide 15
Effects of preheating
RESULTS
No Preheat
Preheated

## Slide 16
Non-Preheated Films
RESULTS

## Slide 17
Preheated Films
RESULTS
Peak 1
Peak 2

## Slide 18
Viscoelastic properties
RESULTS
Film | Preheated | E' (195 oC) [MPa] | T (tand peak 2) [oC] | tand peak 2
Neat | N | 2382 ±127 | 165 ± 3 | 0.216 ± 0.045
 | Y | 2289 ± 152 | 169 ± 4 | 0.213 ± 0.034
Neutralized | N | 4143 ± 334 | 188 ± 10 | 0.078 ± 0.001
 | Y | 4092 ± 397 | 187 ± 5 | 0.078 ± 0.003
Glutaraldehyde | N | 3264 ± 146 | 168 ± 1 | 0.100 ± 0.013
 | Y | 3061 ± 410 | 181 ± 8 | 0.129 ± 0.045
CA+HT | N | 4479 ± 635 | 131 | 0.096
 | Y | 4612 ± 244 | 165 ± 3 | 0.051 ± 0.004
CA | N | 4727 ± 349 | 130 ± 8 | 0.097 ± 0.026
 | Y | 4348 ± 93 | 167 ± 1 | 0.061 ± 0.005
CV = 100 % × std. dev. / mean
CV(E′) = 5 – 15 %
CV(Tp2) = 1 – 6 %
CV(tandp2) = 4 – 25 %

## Slide 19
RESULTS
Neat – Glutaraldehyde – no significant difference
Heat treated and non heat treated citric acid films – no significant difference
Peak Deconvolution
Peak center
Full Width at Half Maximum
Neutralized – Citric acid films – no significant difference
(FWHM-GLU > FWHM-CA)
Heat treated and non heat treated CA films – no significant difference
Gaussian distribution
Baseline chosen as lowest tand value

## Slide 20
RESULTS
Crosslinking with Glutaraldehyde

## Slide 21: Concluding Remarks & Upcoming Work
Contribution to knowledge on the viscoelastic properties of chitosan by incorporation of different crosslinkers and preheating conditions
No strong evidence of covalent crosslinking - considerations for using catalyst (sodium hypophosphite) to promote this
Investigate further heterogeneous and homogeneous crosslinking with glutaraldehyde; different concentrations, immersion times
Test physicochemical properties (TS, WVP) of chitosan-citric acid crosslinked films

## Slide 22: Thank you for listening

## Slide 23: Clip art references
lobster by Rutmer Zijlstra from the Noun Project
Crab by Icons Producer from the Noun Project
Shrimp by Iconic from the Noun Project
Mushrooms by Bakunetsu Kaito from the Noun Project
Squid by Cristiano Zoucas from the Noun Project
doodle by Kyle Tezak from the Noun Project
protein by Ricardo Moreira from the Noun Project
Pill by Hopkins from the Noun Project
Health by MRFA from the Noun Project
membrane fabric by Olena Panasovska from the Noun Project
Outfall by Luis Prado from the Noun Project
packaged food by Made from the Noun Project
protein powder by ProSymbols from the Noun Project
Beaker by Márcio Duarte from the Noun Project
drop by kareemovic2000 from the Noun Project
tray by Smalllike from the Noun Project

## Slide 24
EXPERIMENTAL