## Slide 1: UV-absorbing Cellulose Nanocrystals as Functional Reinforcing Fillers in Poly (vinyl chloride) Film Zhen Zhang, Gilles Sèbe, Xiaosong Wang, Kam C. Tam
wzhangzhen@gmail.com

## Slide 2: Poly (vinyl chloride) (PVC)
Films
Pipes
Construction
Electronics
Consequences:
Color change: discoloration or bleaching
Mechanical performances: hard & brittle
Issues of PVC:
Low thermal stability: manufacturing
Weathering degradation due to heat and UV light
Objective: Utilisation of Cellulose Nanocrystals (CNCs) as reinforcing agents and stabilisers in PVC
Waste management 2016, 48, 300-14. Polymer Composites 2016, 37 (7), 2171-2183. Polymers 2015, 7 (9), 1767-1788.

## Slide 3: Preparation and UV crosslinking of PCEM-g-CNC
The CNCs should impart reinforcing properties
PCEM is photoactive and is expected to impart UV-absorbing and photo-crosslinking properties
Poly(cinnamoyloxy ethyl methacrylate) (PCEM) grafted at the CNC surface by surface initiated Atom Transfer Radical Polymerization
Macromolecules 2014, 47 (23), 8247-8254. Nature 2005, 434 (7035), 879-882.
The UV absorption of the conjugated C=C bond at 276 nm decreased with time during irradiation----->> cross-linking
PCEM-g-CNC film undergoes photodimerization when irradiated by UV irradiation

## Slide 4: Optical properties of PVC/PCEM-g-CNC films
Transmittance before and after UV irradiation at 365 nm
Transmittance before and after annealing at 80 oC
Thermal stabilizer for PVC: the lowest transmittance reduction in the visible region after heat annealing
Highly transparency in the visible region with the PCEM-g-CNC filler
UV-blocking properties (below 320 nm)
UV-stabilizer for PVC: the lowest transmittance increase in the visible region after UV irradiation

## Slide 5: Mechanical properties of PVC/PCEM-g-CNC films
Tensile testing before and after 24 h UV irradiation at 365 nm
The PCEM-g-CNC filler act as reinforcing agent The mechanical performances of the PVC/PCEM-g-CNC film increase after UV irradiation
PCEM-g-CNC/PVC film: one stone four birds
(1) UV-blocking (2) UV-resistance
(3) Thermal stability (4) Mechanical performance
UV-Absorbing Cellulose Nanocrystals as Functional Reinforcing Fillers in Poly(vinyl chloride) Films. Zhen Zhang, Gilles Sèbe, Xiaosong Wang, and Kam C. Tam. ACS Applied Nano Materials 2018 1 (2), 632-641. DOI: 10.1021/acsanm.7b00126

## Slide 6: Acknowledge
Thanks for your attention
Thanks to supervisors and lab mates.
wzhangzhen@gmail.com