## Slide 1: Detecting Minute Quantities of Nitrated Organic Compounds by Fluorescence Quenching of Pyrene-Labeled Starch Nanoparticles
By: Sanjay Patel
Supervisor: Jean Duhamel
University of

## Slide 2: Outline
Introduction
- General Overview for Nitrated Compound Detection
- Starch Nanoparticles
- Pyrene
Experimental
- Synthesis of Pyrene Labeled Starch Nanoparticles
- Quenching Experiments in DMSO and Water
- Quenching studies on Py-SNP-coated filter paper
Conclusions
Future work
Acknowledgements

## Slide 3: Outline
Introduction
- General Overview for Nitrated Compound Detection
- Starch Nanoparticles
- Pyrene
Experimental
- Synthesis of Pyrene Labeled Starch Nanoparticles
- Quenching Experiments in DMSO and Water
- Quenching studies on Py-SNP-coated filter paper
Conclusions
Future work
Acknowledgements

## Slide 4: General overview: Nitrated Organic Compounds
Security Risks1
 Typically nitrated organic compounds are explosive
Health and Environmental concerns1
 Have toxic and mutagenic effects
 Ground water contaminations
Kou-San, J. and Parales, R. Nitroaromatic Compounds , from Synthesis to Biodegradation Microbiol. Mol. Biol. Rev. 2010, 74. 2, 250-272.

## Slide 5: General Overview: Current detection methods
Ion mobility spectroscopy
 Pros: High sensitivity, high throughput, reliable, robust
 Cons: Cost prohibitive, not portable
Canines
 Pros: Low detection limits (ppt)
 Cons: Expensive to train and maintain, tire, will get distracted
Caygill, J. S.; Davis, F.; Higson, S. P. J. Current Trends in Explosive Detection Techniques. Talanta. 2012, pp 14–29.

## Slide 6: General Overview: Current Research
Analytic instrumentation approach1
 Ion mobility spectroscopy, mass spectroscopy, Raman spectroscopy, etc.
 Pros: Typically are sensitive, selective, and robust
 Cons: Prohibitively expensive, and non-portable
Sensor techniques1,2
 Electrochemical sensors, mass sensors, optical sensors, biosensors and etc
 Pros: Typically are portable, easily operated, cost effective
 Cons: “Expensive” to produce, lack in sensitivity, selectivity, and reliability
Caygill, J. S.; Davis, F.; Higson, S. P. J. Current Trends in Explosive Detection Techniques. Talanta. 2012, pp 14–29.
Singh, S. Sensors-An effective approach for the detection of explosives. J. Hazard. Mater. 2007, 144, 15-28.

## Slide 7: Criteria for a optical sensor
Cost effective
Portable
   Typically they are incorporated into hand held devices
Sensitive and selective
Easily operated and visualized
Singh, S. Sensors-An effective approach for the detection of explosives. J. Hazard. Mater. 2007, 144, 15-28.
Typical optical sensors
Use different substrates as backbones such as linear polymers, nanoparticles, dendrimers, and etc
 Labeled with conjugated polymers, fluorophores, quantum dots or aggregation induced emission pendants (AIEgens)

## Slide 8: Starch Nanoparticles
Starch is a biodegradable polymer composed mainly of amylopectin (highly branched)
Advantages:
- Safe and cost effective nanomaterial based on food-grade starch
- Biodegradable
- Readily adsorbs onto polar surfaces, such as filter paper, glass and etc
Amylopectin

## Slide 9: Why use Pyrene?
High quantum yield and large molar extinction coefficient
Long fluorescence lifetime
Excimer
Hydrophobic

## Slide 10: Outline
Introduction
- General Overview for Nitrated Compound Detection
- Starch Nanoparticles
- Pyrene
Experimental
- Synthesis of Pyrene Labeled Starch Nanoparticles
- Quenching Experiments in DMSO and Water
- Quenching studies on Py-SNP-coated filter paper
Conclusions
Future work
Acknowledgements

## Slide 11: Pyrene labeled Starch Nanoparticles Synthesis
SNPs were dispersed in a 3:1 mixture of DMSO:dimethyl formamide (DMF).
1-Pyrenebutyric acid and dimethylaminopyridine (DMAP) were added to mixture (stirred for 30 minutes).
The mixture was put in an ice bath while diisopropylcarbodiimide (DIC) was added dropwise.
Reaction was stirred for 48 hrs under N2. Next Py-SNPs were purified by precipitation.

## Slide 12: Outline
Introduction
- General Overview for Nitrated Compound Detection
- Starch Nanoparticles
- Pyrene
Experimental
- Synthesis of Pyrene Labeled Starch Nanoparticles
- Quenching Experiments in DMSO and Water
- Quenching studies on Py-SNP-coated filter paper
Conclusions
Future work
Acknowledgements

## Slide 13: Types of Quenching
Reabsorption:
  Whereby the emission or excitation light is absorbed by another molecule.
  Quencher absorption will only affect steady-state fluorescence measurements and not time-resolved fluorescence measurements.
Ks
Py
Q
+
(Py-Q)
f·i(t)
(1-f)·i(t)
Py*
Q
+
Decrease in fluorescence intensity
kq
1/τM
f = fraction of excitation light absorbed by non-complexed pyrene labels

## Slide 14: Steady-State Fluorescence
(PyPy)*
SNP
Py + Py
SNP
(PyPy)
SNP
k
hv
hv
Py + Py*
SNP
τ E-1 s-1
τM-1 s-1

## Slide 15: Steady-State Fluorescence
(PyPy)*
SNP
Py + Py
SNP
(PyPy)
SNP
k
hv
hv
Py + Py*
SNP
τ E-1 + kqE[Q] s-1
τM-1 + kqM[Q] s-1
Q +
+ Q

## Slide 16: Time Resolved Fluorescence
Yields the average time a fluorophore spends in its excited state after excitation.
Ks
Py
Q
+
(Py-Q)
f·i(t)
(1-f)·i(t)
Py*
Q
+
Decrease in fluorescence intensity
kq
1/τM

## Slide 17: Quencher Absorption in DMSO
Dinitrotoluene
Nitrotoluene
Quencher | Concentration range used | Max Abs. at 346 nm | Max Abs. at 375 nm
Nitrotoluene | 0 mM to 4 mM | 1.71 | 0.46
Dinitrotoluene | 0 mM to 3 mM | 1.88 | 0.60
Trinitrotoluene | 0 mM to ___ mM |  | 
Normalized absorption and emission spectra of pyrene
Trinitrotoluene

## Slide 18: Quenching by Nitrotoluene in DMSO
[Nitrotoluene] 
0 mM
4 mM
[Nitrotoluene] 
0 mM
4 mM

## Slide 19: Quenching by Nitrotoluene in DMSO
Ks
Py
Q
+
(Py-Q)
f·i(t)
(1-f)·i(t)
Py*
Q
+
Decrease in fluorescence intensity
kq
1/τM
τo/τ
Fo/F
Fo= Fluorescence intensity of the dye without quencher
τo= Lifetime of the dye without quencher
[Q]= Concentration of quencher
kq= Bimolecular quenching rate constant

## Slide 20: Quenching in DMSO
MNT =
DNT =
TNT =

## Slide 21: Quenching by Nitrotoluene in Water
Water
DMSO
[Nitrotoluene] 
0 mM
4 mM
[Nitrotoluene] 
0 mM
0.3 mM

## Slide 22: Quenching by Nitrotoluene in Water
At 375 nm
At 510 nm

## Slide 23: Quenching by Nitrotoluene in Water
F0= Fluorescence intensity of the dye without quencher
τo= Lifetime of the dye without quencher
[Q]= Concentration of quencher
kq= Bimolecular quenching rate constant
KS= The equilibrium constant for the formation of the ground-state complex
At 510 nm
τo/τ
Fo/F
~0
Ks
Py
Q
+
(Py-Q)
f·i(t)
(1-f)·i(t)
Py*
Q
+
Decrease in fluorescence intensity
kq
1/τM

## Slide 24: Comparison of KS
Dinitrotoluene
Mononitrotoluene
Trinitrotoluene
Increasing Ks

## Slide 25: Outline
Introduction
- General Overview for Nitrated Compound Detection
- Starch Nanoparticles
- Pyrene
Experimental
- Synthesis of Pyrene Labeled Starch Nanoparticles
- Quenching Experiments in DMSO and Water
- Quenching studies on Py-SNP-coated filter paper
Conclusions
Future work
Acknowledgements

## Slide 26: Drop Method: Py-SNP-coated filter papers
N2 in
N2 out
Filter paper
Py-SNP coated paper
1 hour after drying
20 µL of water was added and the steady-state fluorescence spectra were acquired.
Py-SNP in water
N2 in
N2 out
Filter paper
Quenched Py-SNP coated paper
1 hour after drying
20 µL of water was added and the steady-state fluorescence spectra were acquired.
Quencher in ethanol/acetonitrile
Q
Q
Q
Q
Q
Q
Q
Q
Q

## Slide 27: In the absence of quencher
Py-SNP
Ethanol + Quencher
< wF0/eF0>
wF0
eF0
In the presence of quencher
wF0
eF
(wF0/eF)

## Slide 28
It should be noted a change in the fluorescence intensity was observed when going between water and ethanol or acetonitrile. To account for this, all wF0/eF ratios were normalized to the average change in the fluorescence intensity in the absence of quencher.

## Slide 29: Quenching studies on filter paper
Mononitrotoluene
40 (± 14) ng per mm2
Dinitrotoluene
21 (± 8) ng per mm2
Trinitrotoluene
2 (± 0.6) ng per mm2
Naphthalene
(no quenching)

## Slide 30: Outline
Introduction
- General Overview for Nitrated Compound Detection
- Starch Nanoparticles
- Pyrene
Experimental
- Synthesis of Pyrene Labeled Starch Nanoparticles
- Quenching Experiments in DMSO and Water
- Quenching studies on Py-SNP-coated filter paper
Conclusions
Future work
Acknowledgements

## Slide 31: Conclusions
Actual change in color of the Py-SNP coated filter paper with increasing quencher concentration

## Slide 32: Future Work
Characterize the quenching of Py-SNPs in DMSO with TNT
Conduct quenching studies on the Py-SNP –coated filter papers with picric acid, other common contaminants and explosive compounds to demonstrate its selectivity.
Optimize the Py-SNP-coated filter paper

## Slide 33: Acknowledgements
Supervisor: Jean Duhamel
Lu Li and Damin Kim
The Duhamel Group
University of