## Slide 1: Synthesis of Water Dispersible Polypyrrole (PPy) Nanowires
Pengxiang Si

## Slide 2: Synthesis of water dispersible polypyrrole (PPy) nanowires
Cetrimonium bromide (CTAB)
2CTA++S2O82-
(CTA)2S2O8 ↓
n(CTA)2S2O8 ↓+
+
SO42-
Colloid and Polymer Science, 287(11), 1325–1330.
1M HCl
dopamine
APS
Polypyrrole (PPy)

## Slide 3: Synthesis of water dispersible polypyrrole (PPy) nanowires
Stankiewicz, P. (2007). 318(OCTOBER), 426–431.
water
0.075 DA/Py mole ratio
Z-Potential=
-40.8±1.7mV

## Slide 4: Synthesis of water dispersible polypyrrole (PPy) nanowires
0 DA/Py mole ratio
0.075 DA/Py mole ratio
0.15 DA/Py mole ratio
0.075 DA/Py mole ratio
Nano-wire Morphology
Good dispersity and stability in water
Good conductivity (3.7 S/cm)
1μm
1μm
1μm
Compress to pellet