## Slide 1: Characterization of Hydrophobically Modified Starch NanoParticles by Pyrene Fluorescence
Damin Kim, Ryan Amos, Jean Duhamel*, Mario Gauthier*
University of Waterloo
Notes: 19 sec

## Slide 2: Outline
1. Background
1.1 Starch
1.2 Starch NanoParticle
1.3 Pyrene Fluorescence
2. Loading Capacity of HM-SNP
3. The Level of Protection of HM-SNPs
4. Effect of Alkyl Chain Length
5. Conclusions
6. Future Work
7. Acknowledgements
Notes: 8sec

## Slide 3: Background:Starch
Properties
Biodegradable
Biocompatible
Non toxic
Adundant
Economical and Environmental friendly
Amylose
Amylopectine
1,4 glycosidic bond
1,4 glycosidic bond
1,6 glycosidic bond
Notes: present limitations: high viscosity, susceptibility to retrogradation, limited digestibility for some, and limited solubility for others.
Most native starch has limitation for the industrial use and need to be modified.
52sec

## Slide 4
Background:Starch NanoParticles
Starch Nanoparticles (SNPs): Prepared by EcoSynthetix by extruding starch
Smaller than 100 nm
Dispersed in water
Able to swell
Having hydroxyl groups that can undergo chemical modification
Starch Granule
  Starch NanoParticle (SNP)
Notes: One of modification of starch was done by company called ecosynthetix via extrusion process.
Current application of snp is for paper coating. Hydrophobic modification with oh on snp will generate amphiphilicity and expects to use as hydrophobic carrier
34 sec

## Slide 5
Scheme 1. The hydrophobic modification of SNP with hexanoic and propionic acid.
Hydrophobically Modification of SNPs
Functional Group | DS
Propionic Acid (C3) | 0.03
 | 0.05
 | 0.15
 | 0.20
 | 0.25
Functional Group | DS
Hexanoic Acid (C6) | 0.03
 | 0.05
 | 0.08
 | 0.09
 | 0.10
 | 0.12
 | 0.15
Increase in DS
Absence of hydrophobic microdomain
Generation of hydrophobic microdomains
Notes: the formation of hydrophobic microdomain opens a gate to the potential use of HM-SNPs as a hydrophobic carrier. And the potential increases as hydrophobicity of hm-snp is good enough to attract hydrophobic molecules. The hydrophobicity of hm-SNP was evaluated with pyrene fluorescence.
43 sec

## Slide 6: Pyrene Fluorescence
Chart: Wavelength, nm
I1/I3 ~ 1.8 in water (---)
I1/I3 ~ 0.6 in Cyclohexane (ㅡ)
s0
s1
2
1
0
Vibronic state
Electronic state
(0,2)
(0,0)
Large molar extinction coefficient and quantum yield
Low solubility in water (~ 0.7 mM)
Sensitive to the local environment
  lifetime
  (~ 350 ns in unaerated organic solvent)
  Polarity (I1/I3)

## Slide 7
Chart: Time, ns
Chart: Time, ns
Chart: Wavelength, nm
Chart: Wavelength, nm
7
Non-BG corrected spectrum
Fluorescence of SNP (~ 30 ns)
Fluorescence of Pyrene
(> 300 ns)
SNP Fluorescence
Fluorescence emission of SNP:
The natural fluorescence of the HM-SNPs distorts the fluorescence of pyrene and a background correction must be applied.
BG-corrected
spectrum
2. Fluorescence Decay of SNP: The decay analysis program needs an extra parameter to account the fluorescence decay of SNP.
SNP dispersion
Py in SNP dispersion

## Slide 8: Outline
1. Background
2. Loading Capacity of HM-SNP
3. The Level of Protection of HM-SNPs
4. Effect of Alkyl Chain Length
5. Conclusions
6. Future Work
7. Acknowledgements
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Notes: Experiments were designed to demonstrate the concept of using HM-SNP as a hydrophobic carrier by pyrene fluorescence. One of essencial concept as a hydrophobic carrier is the interaction between the carrier and probe. This concept was proved by equilibirium and loading capacity.

## Slide 9: Loading Capacity of HM-SNPs
Chart: Time, ns
HM-SNPs (t ~ 30 ns)
Py in water
(t = 130 ns)
Py bound to HM-SNPs
(t ~ 300 ns)
After rearrangement:
Analysis of the fluorescence decays
The fluorescence decays of pyrene in solutions of HM-SNPs have three components

## Slide 10
Loading Capacity of HM-SNPs
Chart: [C6SNP(0)], g/L
| 6.8899196568266508 | 5.9586344508955644 | 5.2715616973854997 | 4.9844146344828895 | 4.2694232273951815 | 3.7130101666500139 | 3.1105941006356539 | 2.371504964301709 | 1.8809321595376789 | 1.312847157596386 | 0.80565001127687441 | 0.46773697324299662
DS= 0.08 | 0.91295 | 0.7506 | 0.69137 | 0.68775 | 0.53479 | 0.48053 | 0.43764 | 0.33525 | 0.25629 | 0.17351 | 0.078732 | 0.0032302
DS= 0.09 | 0.82845 | 0.61573 | 0.41723 | 0.31119 | 0.24018 | 0.14756 | 0.071751 | 0.035616 | 0.024937 | 0.0056557 | 0.022934
DS= 0.10 | 0.69467 | 0.61069 | 0.44633 | 0.37377 | 0.23857 | 0.20594 | 0.12326 | 0.096094 | 0.07026 | 0.031602 | 0.01809 | -0.023609 | 0.0048849
DS= 0.12 | 1.2521 | 1.0163 | 0.88049 | 0.69339 | 0.65401 | 0.4233 | 0.35841 | 0.21448 | 0.090178
DS= 0.15 | 1.3853 | 1.0986 | 0.84627 | 0.61139 | 0.39792 | 0.26068 | 0.16411 | 0.073596 | -0.004695
Chart: ffree/fbound
| 2.3273630539939871 | 4.7845147969717807 | 7.3017131669114068 | 9.6316192420569209
 | 1.7078 | 1.747 | 1.7981 | 1.841
Fluorescence decays of pyrene were acquired at different [HM-SNPs] and constant [pyrene].
The fbound/ffree ratio increased linearly with increasing C6(x)-SNP(0) concentration, as expected.The slope of these plots yielded KB
The y-intercept of the plot of the I1/I3 was extrapolated to yield ( I1/I3)0 ratio corresponding to pyrene bound to SNP(0).
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Increase in DS

## Slide 11
Chart: Degree of Substitution
| 0 | 2.5000000000000001E-2 | 0.05 | 0.05 | 7.5000000000000011E-2 | 9.0000000000000024E-2 | 0.1 | 0.12000000000000002 | 0.12000000000000002 | 0.15000000000000016
 | 0.049625 | 0.059907 | 0.074406 | 0.11299 | 0.12635 | 0.12716 | 0.17262 | 0.33092 | 0.27603 | 0.49174
0.07 0.10 0.12 0.13 0.05 0.08 0.1 0.12 | 0.11056 | 0.13483 | 0.15639 | 0.24724 | 0.080341 | 0.14377 | 0.17776 | 0.32454
Chart: Degree of Substitution
| 0 | 8.0000000000000043E-2 | 0.1 | 0.12000000000000002 | 0.15000000000000013 | 0.12000000000000002 | 0.13
 | 1.6626 | 1.4709 | 1.4603 | 1.4246 | 1.3142 | 1.4272 | 1.3615
 | 1.4272 | 1.3615 | 1.5208 | 1.4545 | 1.4596 | 1.4399 | 1.3567
Loading Capacity of HM-SNPs
Binding of pyrene to C6(x)-SNP(0) was enhanced with increasing DS of hexanoic acid, resulting in a less polar environment for pyrene.
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Py
Increase in DS

## Slide 12
Chart: Time, min
| 0 | 50 | 105 | 165 | 230 | 288 | 1548 | 1628 | 4488
 | 0 | 0.085386 | 0.19331 | 0.24781 | 0.31711 | 0.34299 | 0.42872 | 0.42732 | 0.40971 | 0.40219
Loading Capacity of HM-SNPs
Loading capacity of pyrene in HM-SNPs was determined with UV-Vis spectrospectroscopy and applying Beer lamber Law.
APy= lePy[Pyrene]
Where APy is the absorbance of pyrene at 336 nm, l is the path length of the absorption cuvette, and ePy is the molar extinction coefficient of pyrene.
Chart: Wavelength
The loading capacity of pyrene in the C6(x)-SNP(0) particles was determined by measuring the absorbance of a C6(x)-SNP(0) dispersion saturated with pyrene crystals. The constant absorbance over time indicated full loading of
pyrene in HM-SNP.
epySNP was determined with absorbance of a known concentration of pyrene
and equalled to 29,600 (± 380) M-1cm-1.
Py
Py
Py
Py
Py
Py
hn
Notes: he interaction between py and snp was quantitatively determined with uv

## Slide 13
Loading Capacity of HM-SNPs
Chart: Degree of Substitution
| 0 | 3.0000000000000002E-2 | 0.05 | 8.0000000000000029E-2 | 9.0000000000000024E-2 | 0.1 | 0.12000000000000002 | 0.12000000000000002 | 0.15000000000000005
 | 0.03188 | 0 | 0.0047795 | 0.056739 | 0.032247 | 0.064268 | 0.065525 | 0.066259 | 0.37323
Chart: Degree of Substitution
| 0 | 2.5000000000000001E-2 | 0.05 | 0.05 | 7.5000000000000011E-2 | 9.0000000000000024E-2 | 0.1 | 0.12000000000000002 | 0.12000000000000002 | 0.15000000000000005
 | 0.049625 | 0.059907 | 0.074406 | 0.11299 | 0.12635 | 0.12716 | 0.17262 | 0.33092 | 0.27603 | 0.49174
 | 0.055341 | 0 | 0.0082968 | 0.098492 | 0.055977 | 0.11156 | 0.11374 | 0.11502 | 0.64788
Where ePySNP = 29,600 (± 380) M-1cm-1
The [Py]bound and [Py]W concentrations determined from the absorption spectrum were also used to determined KB which was compared to KB obtained from the fluorescence decay analysis.
The absorbance of pyrene free in water was subtracted from the total absorbance of pyrene in the aqueous dispersion of HM-SNPs.
○ Absorbance
● Fluorescence
Notes: epySNP was determined with absorbance
of a known concentration of pyrene
and equalled to 29,600 (± 380) M-1cm-1.

## Slide 14: Outline
1. Background
2. Loading Capacity of HM-SNP
3. The Level of Protection of HM-SNPs
3.1 Quenching of Pyrene by Oxygen
3.2 Quenching of Pyrene by Nitromethane
4. Effect of Alkyl Chain Length
5. Conclusions
6. Future Work
7. Acknowledgements
Py
Py
Py
Py
Q
Py
Q
Py
Q
Q
Q
Q
Notes: Another improtant factor as hydrophobic carrier is whether it can protect its probe from external obstacle. The level of protection of pyrene of modified snp was simulated by quenching study.

## Slide 15
Chart: Wavelength, nm

15
15
15
Quenching
Quenching: an excited fluorophore loses energy to a quencher and comes back to its ground state without emitting a photon of light
[Nitromethane]
0 mM
10 mM
Chart: Time, ns
[Nitromethane]
=0 mM
5 mM
Notes: In quenching study where a fluorophore and a quencher remain same, the kq is dependent on the probability of quenching. Longer lifetime of pyrene indicates more inefficient quenching by oxygen. When pyrene bound to SNP, orientation of pyrene is more restricted and the probability of quenching decreases. The poor probability of quenching reflected in longer lifetime of pyrene in SNP dispersion compared to water.

## Slide 16
16
16
Lifetime of pyrene
16
t and t0 are lifetime of fluorophore in presence/absence of a quencher, respectively
Quenching of Pyrene by Oxygen
The efficiency of quenching can be described with bimolecular quenching rate constant, kq
Where RF and RQ are the radii of the fluorophore and quencher and DQ is diffusion coefficient of a quencher. p is the probability of quenching.
Increase in to is a result of the increase of the microviscosity experienced by the pyrene molecule bound to HM-SNPs
Chart: Degree of Substitution
| 0 | 2.5000000000000008E-2 | 5.0000000000000017E-2 | 5.0000000000000017E-2 | 8.0000000000000029E-2 | 9.0000000000000024E-2 | 0.1 | 0.12000000000000002 | 0.12000000000000002 | 0.15000000000000005
 | 207.1912 | 240.5511 | 259.9023 | 260.4421 | 271.2212 | 266.515 | 290.9088 | 283.7056 | 287.3234 | 307.898
 | 245.5613 | 262.0871 | 279.2211
 | 258.6082 | 262.0076 | 279.5861 | 293.6668
Notes: In quenching study where a fluorophore and a quencher remain same, the kq is dependent on the probability of quenching. Longer lifetime of pyrene indicates more inefficient quenching by oxygen. When pyrene bound to SNP, orientation of pyrene is more restricted and the probability of quenching decreases. The poor probability of quenching reflected in longer lifetime of pyrene in SNP dispersion compared to water.

## Slide 17: Quenching of Pyrene by Nitromethane
Linear Stern Volmer plot obtained from quenching pyrene in water while the downward plot was obtained from quenching pyrene in the aqueous dispersion of HM-SNP. The downward Stern Volmer Plot indicates the protection of pyrene from quenching.
Chart: [Nitromethane], M
| 0 | 6.3509754725148712E-4 | 1.341218741217994E-3 | 1.9366722307652578E-3 | 2.5507759880674646E-3 | 3.1427169198963117E-3 | 3.6920564907608907E-3 | 4.8166841126586687E-3 | 6.3934662601978871E-3 | 7.9317462114240986E-3 | 1.0282203093911946E-2
 | 1 | 1.1484 | 1.5483 | 2.0431 | 2.2389 | 2.7708 | 3.1069 | 3.3268 | 3.6043 | 4.4357 | 5.7381
 | 1 | 1.1446 | 1.6446 | 2.0377 | 2.4209 | 2.6556 | 2.9072 | 3.2766 | 4.2808 | 4.7819 | 5.6832
Chart: [Nitromethane], M
| 0 | 0 | 5.6548784857611415E-4 | 1.1185683688290382E-3 | 1.1517343891923359E-3 | 1.5466799998538909E-3 | 1.6211711245149361E-3 | 2.1018255232576294E-3 | 2.1660231524194885E-3 | 2.5634576816452393E-3 | 2.6591423771603812E-3 | 3.0760874596590642E-3 | 3.2038592587815755E-3 | 4.0800952247851806E-3 | 4.2788206450591745E-3 | 5.0674651648190665E-3 | 5.2456885291053794E-3 | 6.6834478561415998E-3 | 8.4843173787686986E-3
 | 1 | 1 | 1.4287 | 1.994 | 2.1408 | 2.3864 | 2.381 | 3.1462 | 3.0478 | 3.5647 | 3.523 | 3.6118 | 3.8745 | 4.4263 | 5.5555 | 5.8272 | 5.9381 | 6.9737 | 8.6959
 | 1 | 1 | 1.5537 | 2.0232 | 2.0611 | 2.4531 | 2.325 | 2.9309 | 2.8807 | 3.3027 | 3.5023 | 3.8286 | 3.8894 | 4.2961 | 4.7411 | 5.3145 | 5.6377 | 6.5032 | 7.8593
Water
Quenching of pyrene by a water soluble quencher, nitromethane
kq of pyrene by nitromethane was determined with fluorescence decays at the different [nitromethane].
Aqueous Dispersion
of HM-SNP
Py
Py
Py
Py
Q
Py
Q
Py
Q
Q
Q
Q

## Slide 18
The Level of Protection of HM-SNPs
Chart: [Nitromethane], M
| 0 | 2.9558480171504585E-4 | 6.2157510113170509E-4 | 9.3328154090336593E-4 | 1.2497785053398999E-3 | 1.5850571059672289E-3 | 2.151289844424763E-3 | 2.9587596729409396E-3 | 3.9724186592663639E-3 | 5.2860915198694762E-3
DS= 0 | 1 | 1.072 | 1.0751 | 1.4989 | 1.4173 | 1.4743 | 1.6639 | 1.9476 | 2.3963 | 2.8886
DS=0.05 | 1 | 1.1379 | 1.2223 | 1.4514 | 1.4518 | 1.5484 | 1.6199 | 1.7317 | 1.7573 | 1.9199 | 1.9941 | 2.2081 | 2.2839 | 3.0003
DS=0.08 | 1 | 1.1186 | 1.2209 | 1.2673 | 1.3793 | 1.441 | 1.5643 | 1.6854 | 1.8342 | 1.9872 | 2.1765 | 2.4615
DS=0.09 | 1 | 1.1022 | 1.2354 | 1.2958 | 1.4162 | 1.5002 | 1.6267 | 1.8033 | 1.9156 | 2.0846 | 2.4499
DS=0.10 | 1 | 1.13 | 1.209 | 1.2937 | 1.4527 | 1.6052 | 1.5596 | 1.6128 | 1.7087 | 1.8681 | 2.0845 | 2.3066
DS=0.12 | 1 | 1.0655 | 1.1428 | 1.2708 | 1.3445 | 1.4629 | 1.5893 | 1.706 | 1.7837 | 1.9643 | 2.2201
DS=0.12 | 1 | 1.1122 | 1.2572 | 1.4257 | 1.5572 | 1.6785 | 1.7957 | 2.125 | 2.4196 | 2.8373 | 3.0914
DS=0.15 | 1 | 1.0865 | 1.1346 | 1.2125 | 1.2904 | 1.3547 | 1.436 | 1.5119 | 1.7113 | 1.8275
Chart: Degree of Substitution
| 3.0000000000000002E-2 | 0.05 | 9.0000000000000024E-2 | 0.1 | 0.12000000000000002 | 0.15000000000000013 | 0
 | 0.066202 | 0.08884 | 0.085439 | 0.036802 | 0.039492 | 0.019605 | 0.2404
kq decreases with increasing DS of hexanoic acid. This agrees with experiment result obtained with to. Pyrene experiences more viscous environment with increasing DS. The level of protection is independent from the DS.
kq of pyrene by nitromethane was determined with lifetime of pyrene corresponding to the pyrene accessible to nitromethane.
Chart: Degree of Subsitution
| 0 | 0.05 | 8.0000000000000029E-2 | 9.0000000000000024E-2 | 0.11 | 0.12000000000000002 | 0.12000000000000002 | 0.15000000000000005
 | 1.75 | 1.4415 | 1.1276 | 1.0914 | 0.83222 | 0.8603 | 0.89164 | 0.54521
 | 1.054 | 0.76623 | 0.75176
 | 1.4206 | 0.82733 | 0.90088 | 0.73265

## Slide 19: Outline
1. Background
2. Loading Capacity of HM-SNP
3. The Level of Protection of HM-SNPs
4. Effect of Alkyl Chain Length
5. Conclusions
6. Future Work
7.Acknowledgements
VS

## Slide 20
Chart: Degree of Substitution
| 0 | 2.5000000000000001E-2 | 0.05 | 0.05 | 7.5000000000000011E-2 | 9.0000000000000024E-2 | 0.1 | 0.12000000000000002 | 0.12000000000000002 | 0.15000000000000013
 | 207.1912 | 240.5511 | 259.9023 | 260.4421 | 271.2212 | 266.515 | 290.9088 | 283.7056 | 287.3234 | 307.898
 | 220.3748 | 201.409 | 205.44 | 222.97 | 219.7787
 | 258.0932 | 265.4935 | 280.1192 | 294.5354
Chart: Degree of Substitution
| 0 | 3.0000000000000002E-2 | 0.05 | 8.0000000000000043E-2 | 9.0000000000000024E-2 | 0.1 | 0.12000000000000002 | 0.12000000000000002 | 0.15000000000000013
 | 1.96 | 1.5148 | 1.3036 | 1.1276 | 1.0462 | 0.89165 | 0.84963 | 0.89485 | 0.63454
 | 1.054 | 0.90278 | 0.74125 | 0.72413
 | 1.4266 | 1.9418 | 1.7085 | 1.3663 | 1.4611
Effect of Alkyl Chain Length
Chart: Degree of Substitution
| 0 | 2.5000000000000001E-2 | 0.05 | 0.05 | 7.5000000000000011E-2 | 9.0000000000000024E-2 | 0.1 | 0.12000000000000002 | 0.12000000000000002 | 0.15000000000000016
 | 0.049625 | 0.059907 | 0.074406 | 0.11299 | 0.12635 | 0.12716 | 0.17262 | 0.33092 | 0.27603 | 0.49174
 | 0.11626 | 0.07 | 0.14
0.07 0.10 0.12 0.13 0.05 0.08 0.1 0.12 | 0.11056 | 0.13483 | 0.15639 | 0.24724 | 0.080341 | 0.14377 | 0.17776 | 0.32454
Smaller KB, shorter to, higher kqSNP indicated that pyrene experiences polar and less viscous environment in C3-SNPs than in C6SNPs
Increase in DS
C6-SNP
C3-SNP
C6-SNP
C6-SNP
C6-SNP
C3-SNP
C3-SNP
C3-SNP
Notes: increase

## Slide 21: Outline
1. Background
2. Loading Capacity of HM-SNP
3. The Level of Protection of HM-SNPs
4. Effect of Alkyl Chain Length
5. Conclusions
6. Future Work
7. Acknowledgements

## Slide 22: Conclusions
SNPs were hydrophobically modified with propionic (C3) and hexanoic (C6) anhydride and
characterized with pyrene fluorescence.
The hydrophobicity of the HM-SNPs increased with increasing DS of hydrophophobic pendant and the length of the alkyl chain. As DS of pendants and alkyl chain length increases, more vis-cous and hydrophobic microdomains were generated by the HM-SNPs as demonstrated by
    an increase in KB
    a decrease in to, kq and (I1/I3)o
More hydrophobic microdomains can be generated by maintaining a same DS and increasing
the length of the hydrophobic alkyl chain length than by increasing the DS of a shorter alkyl
chain.
The level of protection and loading capacity of pyrene were not improved much by the
hydrophobic modification of the SNP with C3 and C6 pendants.

## Slide 23: Acknowledgments
Prof. Jean Duhamel
Prof. Mario Gauthier
Prof. Michael Tam
Lu Li and Ryan Amos
Duhamel and Gauthier’s group members
All coworkers from EcoSynthetix Projects