## Slide 1: Fluorescently Labeled Latex Particles to Monitor Film Formation
May 3, 2017
Victoria Hisko
Prof. Mario Gauthier & Prof. Jean Duhamel
Department of Chemistry
University of Waterloo

## Slide 2: Goals?
The goal of this project is to be able determine whether a latex paint film has formed properly through steady-state fluorescence
The film formation process will impact the adhesion, mechanical properties, and surface hardness
Valspar Paint, Chicago, IL
Notes: If the latex particles fail to fuse together, microscopic channels will remain in the final paint film, allowing water and electrolytes to move through the film with greater ease. Via http://www.industrialpaintquality.com/education/inthecan/vs03.html

## Slide 3: Film Formation From Latex Particles
Films must be annealed above the minimum film formation temperature (MFT) for the particles to coalesce properly
If the film remains below the MFT, it will have poor mechanical properties and appear fragile or powdery

## Slide 4: Interparticle diffusion
In the last two steps, what is actually happening is interparticle diffusion and entanglement of the polymer chains to produce a homogenous film
The film properties depend on this diffusion
More extensive diffusion will produce a better film
Notes: More diffusion = better film

## Slide 5: Pyrene
Pyrene is a fluorophore which is typically excited at 344 nm.
The IE/IM ratio is proportional to the local pyrene concentration
Chart: Wavelength (nm)
IE
IM
Chart: Time (ns)

## Slide 6: Project Objectives
The main goal of this project is to be able to monitor film annealing
Pyrene is too hydrophobic alone for incorporation
Oligo(ethylene glycol) units can be added in the pyrene monomer to increase its hydrophilicity
Notes: Before film coalescence, there will be a high local pyrene concentration, leading to blue-green excimer emission.
After film coalescence, the fluorescently labelled polymers will disperse, leading to a lower local pyrene concentration and a predominantly blue emission

## Slide 7: The Monomer
n
Too few ethylene glycol units will not allow efficient incorporation of the monomer into the latex particles
Too many units will lead to crosslinking and/or will modify the properties of the latex
Notes: Tg change  not really monitoring the native latex

## Slide 8: PyEGnOH
Tosylation & Coupling
a)
Ag2O
DCM
+
b)
+
NaH
+
DMF
65oC
Anionic Polymerization
n
+
n
n
n
n
+
THF
n

## Slide 9: PyEGnMA
After the synthesis of PyEGnOH, synthesizing PyEGnMA (or the PyLM) follows the same path
Working with PyEG7MA
Notes: ROH : O attacks C=O in anydride C-O goes back to C=O then cuts other C-O bond in anhydride
DMAP(?) takes on extra proton from ROH+ = ester + H-DMAP?

## Slide 10: Monomer Synthesis: NMR Analysis
n
n
a
{
b
a
{
b
c
d
a
b
Py
a
a
d
c
b
Py

## Slide 11: The Polymer
The desired polymer is a copolymer of n-butyl methacrylate of the pyrene-containing monomer
n

## Slide 12: Emulsion Polymerization
Batch emulsion polymerization is when all the ingredients are placed in the reactor before the reaction
A semi-batch system was used for this project
Initiator: Ammonium persulfate
Surfactant: Sodium docusate salt (AOT)
Chain Transfer Agent: Dodecanethiol (0.3 mg CTA/g monomer)
Notes: Purpose of CTA & Crosslinking

## Slide 13: Property Modification?
For longer EGn linkers and higher labelling levels, the properties of native poly(BuMA) could be modified
Chart: Temperature (oC)

## Slide 14: Film Formation
Once the labeled latex is synthesized, it is mixed with an unlabeled latex of poly(BuMA) having the same molecular weight
The film is dried overnight, then annealed above the MFT
The resulting film is analyzed by steady state fluorescence after different annealing times

## Slide 15: Change in Steady State Fluorescence with Annealing time
Chart: Wavelength (nm)
Increase annealing time

## Slide 16: Change in Steady State Fluorescence with Irradiation
Chart: Wavelength (nm)

## Slide 17
Chart: Wavelength (nm)
Chart: Wavelength (nm)
Irradiation
Annealing

## Slide 18
Chart: Irradiation Time (minutes)
| 0 | 1 | 2 | 3 | 4 | 5 | 10
ND 0.3 - 1.7e5 | 1 | 0.9915 | 0.98084 | 0.96157 | 0.95657 | 0.9433 | 0.91655
Remi's - 8e5 | 1 | 1.0014 | 1.0033 | 1.0058 | 1.0012 | 1.0047 | 1.0067
Chart: Irradiation Time (minutes)
| 0 | 1 | 2 | 3 | 4 | 5 | 10
Blank - 3.7e5 | 1 | 0.99554 | 0.98599 | 0.96563 | 0.95156 | 0.93364 | 0.87259
Blank - 1.6e5 | 1 | 1.003 | 0.99378 | 0.99266 | 0.97861 | 0.9682 | 0.93052
Remi's - 8e5 | 1 | 1.0014 | 1.0033 | 1.0058 | 1.0012 | 1.0047 | 1.0067
Chart: Irradiation Time (minutes)
| 0 | 1 | 2 | 3 | 4 | 5 | 10
Blank - 1.6e5 | 1 | 1.003 | 0.99378 | 0.99266 | 0.97861 | 0.9682 | 0.93052
ND 0.3 - 1.7e5 | 1 | 0.9915 | 0.98084 | 0.96157 | 0.95657 | 0.9433 | 0.91655
ND 1.0 - 1.7e5 | 1 | 1.0008 | 0.99937 | 0.99178 | 0.98187 | 0.97564 | 0.94315
ND 1.0 1.6e5 | 1 | 0.99513 | 0.98831 | 0.97602 | 0.96476 | 0.95633 | 0.91244
Remi's - 8e5 | 1 | 1.0014 | 1.0033 | 1.0058 | 1.0012 | 1.0047 | 1.0067
Chart: Irradiation Time (minutes)
| 0 | 1 | 2 | 3 | 4 | 5 | 10
Remi's - 8e5 | 1 | 1.0014 | 1.0033 | 1.0058 | 1.0012 | 1.0047 | 1.0067
Nitrogen - 1.6e5 | 0.99504 | 1 | 1.0118 | 1.0056 | 1.0036 | 0.99992 | 0.99442 | 0.99046 | 0.9864 | 0.98935 | 0.97081
Py3
Py7
↑ Intensity
Neutral Density Filters
Nitrogen

## Slide 19: Pyrene Cleavage
After sitting in solution un-dialyzed, pyrene starts cleaving off
  3.2% labelled  1.6% labelled
Initiator degrading into sulfuric acid, acidity causing cleavage?
  pH of un-dialyzed solution: 3-4
  pH of dialyzed solution: 7.5

## Slide 20: Py-Labeled Monomers Forming Micelles?
PyEG4MA
PyEG7MA
AOT
PyLM

## Slide 21: Py-Labeled Monomers Forming Micelles?
PyEG4MA
PyEG7MA
BuMA
PyLM

## Slide 22
Chart: Time (ns)
Chart: Time (ns)
TR Excimer - THF
TR Excimer - Water
PyLM
In THF, the PyLM is solvated. Pyrene is free, so it takes a long time for Py* to encounter Py, resulting in a long excimer rise time
In water, Py is pre-aggregated, so it forms excimer instantaneously when irradiated
Py + Py Py* + Py (PyPy)* (PyPy)
hv
hv

## Slide 23: Conclusions
PyLMs with 4 - 7 EG units in the linker were synthesized by different methods
Labelling increased from 1.8 mol% to 3.2 mol%
Annealing trials must be conducted under nitrogen atmosphere to avoid degradation
PyLMs may be forming micelles, resulting in a blocky copolymer microstructure
Emulsions must be dialyzed, or the pH must be adjusted immediately to prevent cleavage of the Py labels

## Slide 24: Future Work
Re-synthesize PyEG7MA-labeled polymer
  Synthesis of monomer ✓
  Synthesis of polymer ✓
Perform annealing trials for new polymer under nitrogen atmosphere

## Slide 25: Acknowledgements
Prof. Mario Gauthier
Prof. Jean Duhamel
Remi Casier
All members of Gauthier & Duhamel groups